Supporting information

Corrosion-free electrochemical synthesis of polyaniline using Cu counter electrode in acidic medium

Subhendu Bhandari, Dipak Khastgir*

Rubber Technology Centre, Indian Institute of Technology Kharagpur,

Kharagpur - 721302, India

* Corresponding author

Dipak Khastgir

Rubber Technology Centre, Indian Institute of Technology Kharagpur,

Kharagpur-721302, India

E-mail: khasdi@gmail.com

Ph. No.: +91-3222-283192

Table S1. Corrosion of Cu electrode in different cycles of electrochemical synthesis.

| Sample code | Synthesis cycle | Initial weight of Cu electrode | Weight of Cu electrode after the synthesis cycle | Weight loss of Cu electrode |
| --- | --- | --- | --- | --- |
| P1 | 1st | 33.826 g | 33.765 g | 61 mg |
|  | 2nd | 33.765 g | 33.743 g | 22 mg |
|  | 3rd | 33.743 g | 33.737 g | 6 mg |
| P2 | 1st | 33.712 g | 33.657 g | 55 mg |
|  | 2nd | 33.657 g | 33.637 g | 20 mg |
|  | 3rd | 33.637 g | 33.625 g | 12 mg |
| P3 | 1st | 33.597 g | 33.597 g | 0 |
|  | 2nd | 33.597 g | 33.597 g | 0 |
|  | 3rd | 33.597 g | 33.597 g | 0 |

Figure S1. Cyclic voltammograms of P1 at different scan rates.

Figure S2. Cyclic voltammograms of P2 at different scan rates.

Figure S3. Cyclic voltammograms of P3 at different scan rates.

Figure S4. Galvanostatic charge-discharge profiles of P1 at different current rates.

Figure S5. Galvanostatic charge-discharge profiles of P2 at different current rates.

Figure S6. Galvanostatic charge-discharge profiles of P3 at different current rates.