Supporting Information

A fluorescent Cd(II) based 2D coordination polymer for highly selective detection of nitroaromatics and Hg2+

YU WU*, RUI WANG, YING-LE LIU, YU-LONG LI, YONG-XIANG HE, YI-WEN LIANG, JIAN-HUI MAN and ABHINAV KUMAR*

Figure S1. View of luminescent spectra for H2L, 4,4’-bipy and 1 at room temperature.

Figure S2. View of luminescent spectra for different NACs in 1 (λex = 290 nm).

Figure S3. Fluorescence response of 1 to 2,6-DNT in DMF (λex = 290 nm).

Figure S4. Views of Stern–Volmer plots for 2,6-DNT.

Figure S5. Fluorescence response of 1 to 4-NT in DMF (λex = 290 nm).

Figure S6. Views of Stern–Volmer plots for 4-NT.

Figure S7. Fluorescence response of 1 to 1,3-DNB in DMF (λex = 290 nm).

Figure S8. Views of Stern–Volmer plots for 1,3-DNB.

Figure S9. Fluorescence response of 1 to TNP in DMF (λex = 290 nm).

Figure S10. Views of Stern–Volmer plots for TNP.

Figure S11. Fluorescence response of 1 to 2-NT in DMF (λex = 290 nm).

Figure S12. Views of Stern–Volmer plots for 2-NT.

Figure S13. View of luminescent spectra for different metal ions in 1 (λex = 290 nm).

Thermal analysis

The thermal stabilities of crystalline samples of 1 were measured under a nitrogen atmosphere. 1 has a two-step weight-loss process. The weight loss of 14.1% (calcd 13.7%) in the first step from 35 to 255 °C corresponds to the removal of one coordinated water and seven free water molecules. The second weight loss occurred in a temperature range from 305 to 575 °C, respectively, corresponding to the decomposition of the organic ligands (obsd: 64.8%; calcd: 65.1%). The remaining residue is attributed to the generation of CdO (obsd 22.8%, calcd 24.3%).

Figure S14. View of TGA in 1.

| HOMO 1 | LUMO 1 |
| --- | --- |
| HOMO 1,3-DNB | LUMO 1,3-DNB |
| HOMO NB | LUMO NB |
| HOMO 2,6-DNT | LUMO 2,6-DNT |
| HOMO 2-NT | LUMO 2-NT |
| HOMO 2,4-DNT | LUMO 2,4-DNT |
| HOMO 4-NT | LUMO 4-NT |
| HOMO TNP | LUMO TNP |
| HOMO TNT | LUMO TNT |

Figure S15. HOMO–LUMO energies of the NACs along with 1.

Figure S16. View of UV-vis spectra of H2L and Hg2+.

Figure S17. View of the PXRD pattern of 1 after detection of different explosives.

Table S1. LOD and Ksv values of 1 for analytes.

| Analytes | LOD | Ksv(M-1) |
| --- | --- | --- |
| Hg2+ | 6.16×10-8 mol/L | 8.19×105 |
| TNT | 5.68×10-7 mol/L | 8.89×104 |
| TNP | 1.31×10-5 mol/L | 3.85×103 |
| 4-NT | 2.40×10-6 mol/L | 2.01×104 |
| 2-NT | 2.64×10-5 mol/L | 1.91×103 |
| 2,6-DNT | 1.86×10-6 mol/L | 2.72×104 |
| 1,3-DNB | 6.88×10-6 mol/L | 7.34×103 |

Table S2. Comparison of the detective sensitivity in various Hg2+ sensors.

| Material | Sensitivity | Reference |
| --- | --- | --- |
| Et4N[Co(L)2] | 1×10-5 M | 1 |
| Zn2(dbtdcO2)2(tppe) | 3.33×10-9 M | 2 |
| PCN-224 | 6×10-9 M | 3 |
| {[Cd1.5(C18H10O10)]·(H3O)(H2O)3}n | 2×10-9 M | 4 |
| COF-LZU8 | 25×10-9 M | 5 |
| [Cd(2NH2bdc)(tib)·4H2O·0.5DMA]n | 4×10-8 M | 6 |
| ZIF-60 | 3×10-9 M | 7 |
| 2,9-DMP | 40×10-9 M | 8 |
| 1 | 6.16×10-8 M | This work |

References

[1]	A. Mishra, J.H. Jo, H. Kim, S. Woo, K.W. Chi. ChemPlusChem, 79, 925 (2014).

[2]	N.D. Rudd, H. Wang, E.M.A. Fuentes-Fernandez, S.J. Teat, F. Chen, G. Hall, Y.J. Chabal, J. Li. ACS Appl. Mater. Interfaces, 8, 30294 (2016).

[3]	J. Yang, Z. Wang, Y. Li, Q. Zhuang, W. Zhao, J. Gu. RSC Adv., 6, 69807 (2016).

[4]	P.Y. Wu, Y.H. Liu, Y. Liu, J.R. Wang, Y. Li, W. Liu, J. Wang. Inorg. Chem., 54, 11046 (2015).

[5]	S.Y. Ding, M. Dong, Y.W. Wang, Y.T. Chen, H.Z. Wang, C.Y. Su, W. Wang. J. Am. Chem. Soc., 138, 3031 (2016).

[6]	L.L. Wen, X.F. Zheng, K.L. Lv, C.G. Wang, X.Y. Xu. Inorg. Chem., 54, 7133 (2015).

[7]	F. Xu, L. Kou, J. Jia, X. Hou, Z. Long, S. Wang. Anal. Chim. Acta, 804, 240 (2013).

[8]	F.S. Shan, J.P. Lai, H. Sun, P. Zhang, C. Luo, Y.H. He, H.R. Feng. RSC Adv., 6, 66215 (2016).