Appendix Table 1. The unit-cell volume of Ne as a function of pressure on the MgO-Y17 scale [18].

V(MgO)	  PMgO (GPa)   VNe (Å3)  	 	   V(MgO)  PMgO (GPa)   VNe (Å3)

Run with Au:				              62.29(4)  	42.3(2)   	32.71(6)

62.42(17)	41.6(8)	   	32.80(3)		       62.57(2)		40.9(1)		32.88(4)

61.75(7)		45.1(4)		32.00(3)				62.27(2)		42.4(1)		32.53(15)

60.92(7)		49.6(4)		31.32(2)				62.34(7)		42.0(3)		32.57(6)

60.52(5)		51.9(3)		30.89(7)				62.51(5)		41.1(3)		32.96(8)

60.33(6)		53.0(4)		30.73(6)				62.30(2)		42.2(1)		32.68(6)

59.98(6)		55.1(4)		30.48(6)				62.28(1)		42.3(1)		32.52(11)

58.74(7）	62.8(5)		29.55(3)				61.81(7)		44.7(4)		32.23(12)

59.38(7)		58.7(5)		29.99(2)				62.08(4)		43.3(2)		32.49(7)

59.11(9)		60.4(6)		29.87(6)				61.90(5)		44.3(2)		32.25(2)

58.91(5)		61.7(3)		29.58(4)				61.68(1)		45.4(1)		31.99(6)

57.77(9)		69.4(7)		28.66(4)				61.23(2)		47.9(1)		31.68(6)

58.31(7)		65.7(5)		29.19(2)				60.46(3)		52.2(2)		30.96(4)

58.48(7)		64.5(5)		29.18(18)			59.69(5)		56.8(3)		30.22(5)

54.52(7)		95.2(6)		26.33(7)				59.89(4)		55.6(3)		30.45(5)

54.34(6)		96.7(6)		26.18(2)				59.43(2)		58.4(1)		29.96(2)

54.25(2)		97.6(2)		26.14(3)				58.86(4)		62.0(2)		29.51(2)

54.01(3)		99.8(3)		26.04(9)				58.76(4)		62.7(3)		29.49(10)

53.30(7)		106.5(7)		25.54(2)				58.14(10)	66.8(7)		28.82(5)

52.90(7)		110.5(7)		25.32(7)				58.42(8)		64.9(5)		29.19(3)

52.86(2)		110.9(2)		25.32(12)			58.50(3)		64.4(2)		29.27(14)

52.68(6)		112.7(6)		25.15(14)			58.62(3)		63.6(2)		29.35(2)

52.57(5)		113.9(5)		25.09(7)				61.07(4)		48.7(2)		31.23(7)

52.41(3)		115.5(3)		25.02(7)				61.03(1)		49.0(1)		31.25(4)

52.36(3)		116.1(3)		24.96(7)				56.30(4)		80.3(3)		27.57(3)

52.37(1)		115.9(1)		24.97(7)				55.22(5)		89.1(4)		26.78(2)

52.07(3)		119.2(3)		24.81(11)			54.56(6)		94.8(6)		26.42(3)

51.96(1)		120.4(1)		24.71(9)				53.12(2)		108.3(2)		25.46(8)

53.13(3)		108.2(3)		25.47(18)

Run with Pt:	 	 							52.53(8)		114.3(8)		25.08(15)

63.93(6)		34.4(3)		34.52(12)			51.96(9)		120.3(10)	24.72(7)

63.32(1)		37.2(1)		33.80(12)		   	51.89(10)	121.1(11)	24.67(6)

62.59(2)		40.7(1)		32.91(6)				51.28(5)		127.9(5)		24.33(15)

Supplementary Figure captions:

Figure S1. Comparison of the MgO scales [18,42,45-47] up to 250 GPa.

Figure S2. Isothermal compression of NaCl-B2 from Dorfman et al. [3], with pressures calculated from the MgO-Y17 scale [18]. The curve represents the Vinet fitting for NaCl-B2 with the ambient volume fixed [49]. (Inset) Pressure differences between fitting (PNaCl) and observation (PMgO_Y17).

Figure S3. The R1 line shift of ruby luminescence at high pressure in a He medium from Speziale et al. [46] (gray circle) and Jacobsen et al. [50] (black diamond). The pressure is calculated on the MgO-Y17 scale [18]. (Inset) Pressure differences between fitting (Pruby) and observation (PMgO_Y17).

Figure S4. Comparisons of the (a) MgO, (b) Pt and (c) Au scales [18,19,47,48,52,53] up to 250 GPa. The scales from Ye et al. [18] are selected as references.

Figure S5. The Debye-Grüneisen parameter, D (a), the Debye temperature, D (b) and the Debye thermal pressure, Pth (c) over the unit-cell volume at high pressure for this Ne dataset. (d) The unit-cell volume as a function of pressure with 3rd-order BM (solid curve) and Vinet (dashed curve) EOS fittings at 0 K. P0K = P300K - Pth(V, 300K).

Figure S6. The fitted pressure residue for the modified 3rd-order BM (A) and Vinet (B) EOSs at Pr = 4.7 GPa. These datasets have been presented in Figure 3, and the Pstd values are identical with those in Figure 3.