Electronic Supporting Information

Structures, stabilities and electronic properties of boron-doped silicon clusters B3Sin (n=1-17) and their anions

Cheng-Gang Lia, b, Jin-Hai Gaoa, Jie Zhanga, Wan-Ting Songa, Shui-Qing Liua, Si-Zhuo Gaoa, Bao-Zeng Renb, Yan-Fei Huc d(

a College of Physics and Electronic Engineering, Quantum Materials Research Center, Zhengzhou Normal University, Zhengzhou 450044, China

b School of Chemical Engineering and Energy, Zhengzhou University, Zhengzhou 450001, China

c School of Physics and Electronic Engineering, Sichuan University of Science ＆ Engineering,

Zigong 643000, China

d National Key Laboratory for Shock Wave and Detonation Physics Research, Institute of Fluid

Physics, China Academy of Engineering Physics, Mianyang 621999, China

(Correspondence to: Yan-FeiHu, School of Physics and Electronic Engineering, Sichuan University of Science ＆ Engineering, Zigong 643000, China. E-mail address: yanfei_hu1982@suse.edu.cn

Cartesian cordialities for the lowest-energy structures and low-lying isomers are listed in the paper.

Neutral clusters

B3Si Cluster

B                  0.00000000    0.00000000   -1.86665100

B                  0.00000000    0.88471400   -0.61865000

B                  0.00000000   -0.88471400   -0.61865000

Si                 0.00000000    0.00000000    1.10855400

B3Si2 Cluster

B                  0.00000000    0.00000000    0.38749300

B                  0.00000000    0.78046500   -1.16084100

B                  0.00000000   -0.78046500   -1.16084100

Si                 0.00000000   -1.98713300    0.34539100

Si                 0.00000000    1.98713300    0.34539100

B3Si3 Cluster

B                  0.00000000    0.78374200    0.00000000

B                  0.43737200   -0.83611400    0.00000000

B                  1.55670100    0.38795900    0.00000000

Si                 2.48310400   -1.26628000    0.00000000

Si                -1.71208200    1.76432900    0.00000000

Si                -1.48319100   -0.61790100    0.00000000

B3Si4 Cluster

B                  0.40030000   -1.43473900    0.78867000

B                  0.40030000   -1.43473900   -0.78867000

B                  1.01780500   -0.08421400    0.00000000

Si                -0.05846700    1.58709600    0.00000000

Si                 0.40030000    0.00269800    2.06594500

Si                -1.39156200   -0.53760300    0.00000000

Si                 0.40030000    0.00269800   -2.06594500

B3Si5 Cluster

B                  0.28285900   -0.01058300    0.82857300

B                  0.08818400    1.42656900    0.00000000

B                  0.28285900   -0.01058300   -0.82857300

Si                -0.07921000   -0.86975400    2.50632700

Si                -0.07921000    1.57235400    1.97789700

Si                -0.07921000   -0.86975400   -2.50632700

Si                 0.08330200   -1.90712900    0.00000000

Si                -0.07921000    1.57235400   -1.97789700

B3Si6 Cluster

B                  0.68863800    0.04294700   -0.84092600

B                 -0.88744500    0.17318400   -0.30655000

B                 -0.13448300   -1.32999600   -0.25509300

Si                 2.45772800    0.75802000   -0.23968700

Si                 0.13635500    1.94938000   -0.24861100

Si                 0.62006300   -0.04070500    1.45922200

Si                -2.12134100   -1.45936800   -0.11758500

Si                 1.80969800   -1.62681000   -0.30802500

Si                -2.78347000    0.81729200   -0.04439700

B3Si7 Cluster

B                 -0.67027700    0.20942100   -0.59479000

B                 -0.06610200   -1.33249700   -0.20309300

B                  0.60034200   -0.01372000    0.72439700

Si                 1.25983800    0.04499900   -1.56460900

Si                -1.33724900   -0.22699100    1.60955600

Si                -2.51240200    0.99111700   -0.28700500

Si                -2.03635300   -1.40452200   -0.55065400

Si                 1.86197000   -1.66152800    0.26146800

Si                 2.49030500    0.70409300    0.60522000

Si                 0.32247600    1.95883000   -0.04773200

B3Si8 Cluster

B                 -0.86066900    0.02991600   -0.85580100

B                  0.40806300    0.81595400    0.07149700

B                  0.28776600   -1.02852200   -0.05477500

Si                 2.26887000   -1.33965700   -0.24757200

Si                 2.34883400    1.34410500   -0.10837500

Si                -2.85604800    0.11496500   -0.62660900

Si                -1.20774800   -0.03744600    1.50088900

Si                -1.57404100   -1.90362000   -0.12653300

Si                -1.36988800    1.96996800    0.03300100

Si                 1.06773900    0.06846300   -1.88361200

Si                 1.38115300   -0.15154500    1.75848100

B3Si9 Cluster

B                  0.00000000    1.04768300    0.29861000

B                 -0.90732000   -0.52384200    0.29861000

B                  0.90732000   -0.52384200    0.29861000

Si                 0.00000000    1.68049400   -1.70545500

Si                -1.45535000   -0.84024700   -1.70545500

Si                 1.45535000   -0.84024700   -1.70545500

Si                 0.00000000   -1.53847400    1.97449100

Si                 1.33235800    0.76923700    1.97449100

Si                -1.33235800    0.76923700    1.97449100

Si                 0.00000000   -2.35054600   -0.37568200

Si                 2.03563300    1.17527300   -0.37568200

Si                -2.03563300    1.17527300   -0.37568200

B3Si10 Cluster

B                 -0.11630800    0.82689200    0.52621800

B                 -0.43276400   -0.68171400   -0.36725200

B                  1.48383300    1.37485500    0.33435800

Si                -1.00447400   -0.60148600    1.76761800

Si                -1.95977500    1.74017100    0.89396800

Si                 0.12072300    2.82322500   -0.01424900

Si                 3.24973500    0.51355100    0.22550900

Si                 1.45794700   -0.64340600    1.33102500

Si                -1.79513000   -2.19609100   -0.03267800

Si                -2.43742400   -0.00282800   -1.01925500

Si                -0.25333600    0.98813500   -1.71991400

Si                 1.59531800   -0.63424100   -1.35277500

Si                 0.69257300   -2.52989800   -0.25543700

B3Si11 Cluster

B                 -0.00177100    1.45115700   -0.13761100

B                 -1.33607400    0.32238900   -0.03357700

B                  0.26709600   -0.30860300    0.03084500

Si                 1.48981100    1.03541900   -1.45049600

Si                -1.26467900   -1.56410900   -1.07171000

Si                 0.99191700   -0.95250100    2.09820600

Si                -3.04503100    0.28071400    1.22297000

Si                 2.33273700   -1.21732000    0.11417100

Si                 0.99551100   -1.32413500   -1.88533800

Si                 1.48795500    1.28426400    1.23429600

Si                -1.26906200   -1.33835400    1.33997000

Si                -1.80850400    2.29974700   -0.20010000

Si                -3.04309400    0.03805000   -1.26463600

Si                 3.51484800    0.93503100   -0.08721100

B3Si12 Cluster

B                 -0.12662700   -0.37303700    0.87676400

B                 -0.12662700   -0.37303700   -0.87676400

B                  0.01164400    1.11174200    0.00000000

Si                -1.44777600   -1.18126800   -2.26847100

Si                -1.11957200    1.24507900   -1.95212700

Si                -1.09816000    2.85966400    0.00000000

Si                -1.11957200    1.24507900    1.95212700

Si                -1.44777600   -1.18126800    2.26847100

Si                -1.17894700   -2.07275000    0.00000000

Si                 1.14389100   -1.41503100   -2.15566200

Si                 1.26114600    0.97558400   -1.90385300

Si                 1.53995300    2.53453700    0.00000000

Si                 1.26114600    0.97558400    1.90385300

Si                 1.14389100   -1.41503100    2.15566200

Si                 1.14806500   -2.70077300    0.00000000

B3Si13 Cluster

B                 -0.48984600   -0.77144400   -0.18030600

B                 -0.10682500    0.96411500    0.03603000

B                  1.16775100   -0.20224600   -0.01765200

Si                -1.40884400   -1.51783300   -2.02328500

Si                -0.46846100    2.74517700   -1.11492200

Si                 0.93888600   -1.89200000   -1.46551400

Si                 1.72828600    1.84244400   -0.80348200

Si                -1.00844800   -1.63723500    2.04225400

Si                -0.96450400    2.23239400    1.39900000

Si                 1.00844300   -2.21289600    0.93564200

Si                 1.41680100    1.51279300    1.53511200

Si                 2.86543400   -0.26636600   -1.27266600

Si                 2.75827400   -0.58977800    1.27177700

Si                -2.42336700   -1.68579900    0.24097100

Si                -1.73757200    0.77207100   -1.38000900

Si                -2.90888500    0.70045000    0.69295200

B3Si14 Cluster

B                  0.26319600   -0.53458500    0.90888000

B                 -1.05140800    0.14628000    0.00000000

B                  0.26319600   -0.53458500   -0.90888000

Si                -3.07164700   -0.29602200    0.00000000

Si                 1.69635300    2.84655700    0.00000000

Si                 1.95461600   -0.92655600   -2.04197700

Si                -1.51622200   -1.18058200    1.80781300

Si                 0.35055400   -2.63677500    1.27368100

Si                 0.35055400   -2.63677500   -1.27368100

Si                -0.11407700    2.08155300    1.34764000

Si                -2.04927100    2.04076900    0.00000000

Si                 0.05737300    0.31523200   -2.93399900

Si                 1.95461600   -0.92655600    2.04197700

Si                -1.51622200   -1.18058200   -1.80781300

Si                 2.14758300    0.43255800    0.00000000

Si                 0.05737300    0.31523200    2.93399900

Si                -0.11407700    2.08155300   -1.34764000

B3Si15 Cluster

B                  0.80707900    1.00244300   -0.05723900

B                 -0.50198700   -0.05860900    0.23344700

B                  1.15256000   -0.73125600    0.03723700

Si                 1.56967500    2.70983800    0.87865500

Si                -0.65575700    1.78925600    1.41567000

Si                 2.80250300    0.57710900    0.82332500

Si                -2.78754400    2.35693200    0.10029300

Si                 2.34518200    0.35924600   -1.55236200

Si                -2.72424600   -0.02055600    0.40752700

Si                 2.05419500   -1.34668300    2.02115100

Si                -1.28578400   -0.37074400    2.28665100

Si                 1.07595300    2.42454600   -1.60010700

Si                -1.14990400    1.38636600   -1.41848400

Si                 1.24396400   -1.71179800   -1.94280900

Si                -1.12318500   -0.94988900   -1.75278600

Si                 1.57318400   -2.85158800    0.18887000

Si                -0.65818400   -2.14794500    0.71685800

Si                -2.80064300   -2.28001100   -0.64868300

B3Si16 Cluster

B                  0.08243600    1.29861200   -0.24616500

B                 -0.16179600    0.02334700    0.96087600

B                  0.15484600   -1.05353700   -0.33816200

Si                -1.35593700   -0.29030700   -1.95548300

Si                -1.74302600   -0.45761500    2.41904100

Si                 2.35054500    1.55399300    0.19443200

Si                -0.79253200    2.06595600   -2.04948200

Si                 0.55424900   -0.06324700    3.00059500

Si                -1.75627100   -1.83447200    0.48634300

Si                 0.31938900   -2.01461400   -2.17087800

Si                 1.48873200   -1.46738200    1.23366600

Si                 2.08087500   -0.66443300   -1.46702000

Si                -1.25438300    3.01536500    0.25309700

Si                -2.37416000    0.91354200    0.61210400

Si                -3.41009400   -0.72625900   -0.87897400

Si                 0.10541400   -3.21885500    0.06154500

Si                 3.60285900   -0.58331100    0.36107300

Si                 1.52035200    1.59913300   -1.94608000

Si                 0.63702900    2.07664100    1.71153900

B3Si17 Cluster

B                  0.42599100   -0.91470100   -0.62293900

B                  0.04909100   -0.22276100    0.99546000

B                 -1.23102800   -0.53638500   -0.14209800

Si                 1.90615800   -1.34007700    0.88808000

Si                 3.77988900    0.21259300    0.70119100

Si                 2.46298200    0.61582700   -1.26290300

Si                 1.28090200   -0.95191500   -2.56317400

Si                 1.33677300   -2.83263100   -0.96144800

Si                -0.91474100    0.01983700   -2.25089100

Si                 1.47119600    2.70850800   -1.01652200

Si                -1.44947500   -1.85262000    1.65887500

Si                -2.75949400   -1.36808900   -1.57395800

Si                -0.81378000    2.23224200   -1.33913300

Si                 0.48409000   -1.19888100    2.87130100

Si                -0.99545700   -2.73982400   -0.51370300

Si                 1.84083700    1.63280700    1.01929600

Si                -3.32379000   -0.48933900    0.84688600

Si                -2.36304100    3.39297400   -0.13927100

Si                 0.08613800    1.23139000    2.55623300

Si                -1.75920600    1.32500100    0.99684700

Anionic clusters

B3Si- Cluster

B                  0.00000000    0.84570100   -0.64019500

B                  0.00000000   -0.84570100   -0.64019500

B                  0.00000000    0.00000000   -1.91218500

Si                 0.00000000    0.00000000    1.14020600

B3Si2- Cluster

B                  0.00000000    0.77300000   -1.17260700

B                  0.00000000    0.00000000    0.33398300

B                  0.00000000   -0.77300000   -1.17260700

Si                -0.15184600    1.98535600    0.35914800

Si                 0.15184600   -1.98535600    0.35914800

B3Si3- Cluster

B                  0.00000000    0.78840800    0.00000000

B                  1.57783800    0.39064100    0.00000000

B                  0.48701300   -0.82797900    0.00000000

Si                 2.48410200   -1.23616000    0.00000000

Si                -1.47215400   -0.58179900    0.00000000

Si                -1.74939400    1.69257700    0.00000000

B3Si4- Cluster

B                 -0.33062500   -1.57067700    0.77107900

B                 -0.33062500   -1.57067700   -0.77107900

B                 -0.88614300   -0.15268400    0.00000000

Si                 1.37969400   -0.31220400    0.00000000

Si                -0.33062500   -0.09110300   -2.01863000

Si                -0.16580500    1.67085200    0.00000000

Si                -0.33062500   -0.09110300    2.01863000

B3Si5- Cluster

B                  0.93853600   -0.18037800    0.00000000

B                  0.34008500    1.11312700    0.87598200

B                  0.34008500    1.11312700   -0.87598200

Si                 0.34008500   -0.57375500   -1.98138200

Si                -1.33175900   -0.14457700    0.00000000

Si                 0.54326800   -2.12016400    0.00000000

Si                -0.46978800    2.68158100    0.00000000

Si                 0.34008500   -0.57375500    1.98138200

B3Si6- Cluster

B                 -0.63769300    0.03182500   -0.83419700

B                  0.18233900   -1.27003600   -0.09624300

B                  0.92115200    0.23853700   -0.17449600

Si                -0.20581700    1.94010600   -0.23946900

Si                 2.20349100   -1.36033900   -0.07493000

Si                -0.85622700    0.00648500    1.45864700

Si                -1.73634900   -1.65867000   -0.36189600

Si                -2.49376000    0.67271500   -0.32184500

Si                 2.92230500    0.75672900   -0.06588700

B3Si7- Cluster

B                  0.69029800    0.45397500   -0.37935100

B                 -0.57584800    0.00689200    0.72768900

B                  0.27442600   -1.24914400   -0.07152500

Si                 2.03117500   -1.13287800   -0.93870800

Si                 2.58608000    1.08326600   -0.02127600

Si                 1.56505700   -0.44164700    1.52482700

Si                -1.70140600   -1.74967900    0.20178300

Si                -2.50351300    0.52088100    0.81292100

Si                -0.72778700    1.98134700   -0.19150900

Si                -1.38849000    0.02023600   -1.48690000

B3Si8- Cluster

B                 -1.18827400    0.38372200    0.64035800

B                 -0.69426400   -1.30650200   -0.57774300

B                  0.71666500   -1.29823900    0.31872100

Si                 2.58136300   -0.81475200    0.20476500

Si                -2.57110700   -0.80545900   -0.36078100

Si                -0.54478000    2.29574300    0.46103900

Si                -0.87243600   -1.44598100    1.61852500

Si                 0.56796800    0.57017300    1.89621900

Si                 1.35801800    1.17363900   -0.56228700

Si                 0.90456600   -0.99725300   -1.81902000

Si                -1.00720800    0.81711100   -1.57465100

B3Si9- Cluster

B                  0.00000000    1.00943600    0.31978500

B                  0.87419700   -0.50471800    0.31978500

B                 -0.87419700   -0.50471800    0.31978500

Si                -1.46502100   -0.84583000   -1.73276200

Si                 2.00941500    1.16013600   -0.39468700

Si                 1.46502100   -0.84583000   -1.73276200

Si                -1.32510200    0.76504800    2.01324000

Si                 0.00000000   -1.53009600    2.01324000

Si                 0.00000000    1.69166000   -1.73276200

Si                -2.00941500    1.16013600   -0.39468700

Si                 0.00000000   -2.32027300   -0.39468700

Si                 1.32510200    0.76504800    2.01324000

B3Si10- Cluster

B                 -0.66672500    0.15759800    0.90218700

B                  0.71567800    0.86694500    0.00000000

B                 -0.66672500    0.15759800   -0.90218700

Si                 1.53871400   -0.67721300    1.29214100

Si                -1.28001000    2.05449600    0.00000000

Si                 0.43307300    1.59474500   -1.99121900

Si                -2.07944200   -1.24234800    0.00000000

Si                 1.00189400    2.99442300    0.00000000

Si                 0.43307300    1.59474500    1.99121900

Si                -0.66672500   -1.61750400   -2.03316800

Si                -0.66672500   -1.61750400    2.03316800

Si                 1.53871400   -0.67721300   -1.29214100

Si                -0.03193400   -2.82881900    0.00000000

B3Si11- Cluster

B                 -0.05343500   -0.02940000   -1.45995400

B                 -0.28355700    0.82172500    0.07731500

B                  1.14932800    0.98859500   -0.95599300

Si                -0.23681300   -1.81617200   -0.22124800

Si                -1.97748800   -0.07824300    1.31518300

Si                 3.01588100    0.14238800   -0.15082100

Si                 1.49224400    1.58315800    1.08929200

Si                 1.66728100   -1.03291200   -1.83758700

Si                 0.33796900    2.85509700   -0.60799100

Si                 1.89604300   -1.98427300    0.77322300

Si                 0.32164300   -0.32137500    1.89072200

Si                -2.03889100    0.00852300   -1.34571900

Si                -2.14329400    1.99580700    0.03763200

Si                -2.62469500   -1.98803900   -0.10745900

B3Si12- Cluster

B                 -0.21985000   -0.20600800    0.87748900

B                 -0.21985000   -0.20600800   -0.87748900

B                 -0.00700300    1.25334500    0.00000000

Si                 1.03777700   -3.15703200    0.00000000

Si                 1.01254600   -1.48546300   -1.93431000

Si                 1.31519700    0.89340100   -1.90169200

Si                 1.68233100    2.47533600    0.00000000

Si                 1.31519700    0.89340100    1.90169200

Si                 1.01254600   -1.48546300    1.93431000

Si                -1.51173800   -1.09607500    2.25070600

Si                -1.07697800    1.35756900    2.00798100

Si                -0.93723000    3.04069400    0.00000000

Si                -1.07697800    1.35756900   -2.00798100

Si                -1.51173800   -1.09607500   -2.25070600

Si                -1.10139600   -1.99833600    0.00000000

B3Si13- Cluster

B                 -1.56028600    1.52904500    0.70130100

B                 -0.06553300   -0.85131300   -0.15974300

B                  0.00794400    0.91662500   -0.09954900

Si                 1.20718200    2.34258800   -1.37546500

Si                -0.06951800   -1.16120200    2.02393600

Si                 1.86812900    1.67280000    0.84675300

Si                -1.46231900   -2.10619100   -1.35382800

Si                -2.15188300    0.18617700   -1.24343500

Si                -0.10011600    1.26861300    2.05171800

Si                -1.26072200    2.41059900   -1.08965300

Si                -2.04509300   -1.49433100    0.86954400

Si                 1.74227100   -1.80631100    0.75324800

Si                 1.76082500   -0.00413800   -1.27311400

Si                 1.00789300   -2.30679900   -1.50398400

Si                 3.46280100   -0.12331300    0.41629700

Si                -3.38163800    0.55209400    0.72012200

B3Si14- Cluster

B                 -0.27789400   -0.39433100    0.87165400

B                 -1.07563800    0.92494100    0.00000000

B                 -0.27789400   -0.39433100   -0.87165400

Si                 1.38108900    0.97629900    1.68304200

Si                 1.33950100   -1.30531000    1.97243900

Si                -0.86387400    1.88942200    1.95928400

Si                -0.03459200    2.90128700    0.00000000

Si                 1.38108900    0.97629900   -1.68304200

Si                 2.08849300   -2.61041200    0.00000000

Si                -0.36064600   -2.42146400    0.00000000

Si                -1.11523400   -1.83224900    2.21231800

Si                -2.48983900    0.13649900    1.38739300

Si                -2.48983900    0.13649900   -1.38739300

Si                -1.11523400   -1.83224900   -2.21231800

Si                 2.38611000    2.35259700    0.00000000

Si                -0.86387400    1.88942200   -1.95928400

Si                 1.33950100   -1.30531000   -1.97243900

B3Si15- Cluster

B                 -0.35352400    0.90853600   -0.47490500

B                  0.12374600    0.29337700    1.04643000

B                  0.30548600   -0.84883300   -0.29717400

Si                -3.16962000   -1.42124600   -0.07157400

Si                 3.97837000   -0.53493800   -0.53791900

Si                -1.77590100    2.58439300    0.26876600

Si                -2.18286900    0.38465100    1.14089700

Si                 0.27306000   -1.95541700    1.67891100

Si                -1.05544000   -2.65370400   -0.12207400

Si                -1.68568100   -0.49818200   -1.72271200

Si                -1.34981500    1.87051500   -2.04331600

Si                 0.68498400    2.47079900    0.54996100

Si                -0.68754000   -0.12186200    2.93737500

Si                 2.22829100   -0.81236500    0.92592400

Si                 1.92320500   -0.38338700   -1.61697800

Si                 1.49193300    1.05557300    2.42372600

Si                 1.13375900    1.94315100   -1.77675300

Si                 0.16622700   -2.05408100   -2.13221600

B3Si16- Cluster

B                  0.00000000    1.33888400   -0.21946300

B                  0.00000000   -1.33888400   -0.21946300

B                  0.00000000    0.00000000    0.89665400

Si                 1.15884800   -0.35436300    2.74444000

Si                 3.43219900    0.59018300   -0.70121000

Si                 1.30843300   -2.26666800    1.09682500

Si                 0.85370200    3.24567600    0.56078100

Si                -1.58254000   -2.02244500   -1.42821000

Si                -0.30227800    1.17186400   -2.40295800

Si                -1.87871600   -1.13396200    1.05475800

Si                -1.15884800    0.35436300    2.74444000

Si                 1.58254000    2.02244500   -1.42821000

Si                 2.16444600   -1.49268900   -1.00616300

Si                -2.16444600    1.49268900   -1.00616300

Si                -0.85370200   -3.24567600    0.56078100

Si                 0.30227800   -1.17186400   -2.40295800

Si                -3.43219900   -0.59018300   -0.70121000

Si                 1.87871600    1.13396200    1.05475800

Si                -1.30843300    2.26666800    1.09682500

B3Si17- Cluster

B                  0.45137400    0.78856900   -0.31604900

B                  1.85678500   -0.14581300   -0.03371000

B                 -0.86234300    0.36796400    0.80069300

Si                -1.41910900   -1.73208800    0.47429300

Si                 1.67120600    1.67524000    1.17876900

Si                -1.07184900    2.22252700   -0.77273000

Si                 1.59015100    0.66819400   -2.10521500

Si                -0.44086200   -2.69489900   -1.52512700

Si                 1.79219300   -1.53134600    1.57873200

Si                -2.96045000    0.22231600   -0.03985800

Si                 1.73443800   -2.20943000   -0.59620300

Si                -0.41249000   -1.20305500    2.59250400

Si                -3.77771100   -1.91007100    0.46491600

Si                 3.56754100    0.14338100    1.16248100

Si                -2.17645100    2.02479900    1.33731400

Si                -0.54578700   -0.39736800   -2.10457700

Si                -2.47031500    1.01114800   -2.33706700

Si                 3.49936400   -0.66337800   -1.27234600

Si                -0.29582600    1.22822100    2.73280900

Si                 1.19959400    2.78483900   -0.92974400

Table S1 the local and total magnetic moments of per atom for the lowest energy structures of B3Sin (n=1-17) clusters.

B3Si

| Atom | μs | Atom | μs | Σμs |
| --- | --- | --- | --- | --- |
| B | -0.35 | Si | -0.13 | -1.00 |
| B | -0.26 |  |  |  |
| B | -0.26 |  |  |  |

B3Si2

| Atom | μs | Atom | μs | Σμs |
| --- | --- | --- | --- | --- |
| B | -0.29 | Si | -0.09 | -1.00 |
| B | -0.27 | Si | -0.09 |  |
| B | -0.27 |  |  |  |

B3Si3

| Atom | μs | Atom | μs | Σμs |
| --- | --- | --- | --- | --- |
| B | -0.01 | Si | -0.20 | -1.00 |
| B | -0.02 | Si | -0.35 |  |
| B | -0.22 | Si | -0.21 |  |

B3Si4

| Atom | μs | Atom | μs | Σμs |
| --- | --- | --- | --- | --- |
| B | -0.23 | Si | -0.43 | -1.00 |
| B | -0.23 | Si | 0.01 |  |
| B | -0.02 | Si | -0.13 |  |
|  |  | Si | 0.01 |  |

B3Si5

| Atom | μs | Atom | μs | Σμs |
| --- | --- | --- | --- | --- |
| B | 0.02 | Si | -0.04 | -1.00 |
| B | -0.30 | Si | -0.09 |  |
| B | 0.02 | Si | -0.04 |  |
|  |  | Si | -0.50 |  |
|  |  | Si | -0.09 |  |

B3Si6

| Atom | μs | Atom | μs | Σμs |
| --- | --- | --- | --- | --- |
| B | -0.04 | Si | -0.12 | -1.00 |
| B | 0.02 | Si | 0.01 |  |
| B | -0.01 | Si | -0.10 |  |
|  |  | Si | -0.30 |  |
|  |  | Si | -0.01 |  |
|  |  | Si | -0.45 |  |

B3Si7

| Atom | μs | Atom | μs | Σμs |
| --- | --- | --- | --- | --- |
| B | 0.00 | Si | -0.14 | -1.00 |
| B | 0.02 | Si | -0.38 |  |
| B | -0.01 | Si | -0.17 |  |
|  |  | Si | -0.23 |  |
|  |  | Si | -0.09 |  |
|  |  | Si | -0.01 |  |
|  |  | Si | 0.00 |  |

B3Si8

| Atom | μs | Atom | μs | Σμs |
| --- | --- | --- | --- | --- |
| B | 0.02 | Si | -0.41 | -1.00 |
| B | -0.05 | Si | -0.18 |  |
| B | -0.03 | Si | -0.12 |  |
|  |  | Si | -0.01 |  |
|  |  | Si | -0.07 |  |
|  |  | Si | -0.11 |  |
|  |  | Si | -0.01 |  |
|  |  | Si | -0.04 |  |

B3Si9

| Atom | μs | Atom | μs | Σμs |
| --- | --- | --- | --- | --- |
| B | -0.03 | Si | -0.24 | -1.00 |
| B | -0.03 | Si | -0.24 |  |
| B | -0.03 | Si | -0.24 |  |
|  |  | Si | -0.08 |  |
|  |  | Si | -0.08 |  |
|  |  | Si | -0.08 |  |
|  |  | Si | 0.01 |  |
|  |  | Si | 0.01 |  |
|  |  | Si | 0.01 |  |

B3Si10

| Atom | μs | Atom | μs | Σμs |
| --- | --- | --- | --- | --- |
| B | -0.04 | Si | 0.00 | -1.00 |
| B | -0.05 | Si | -0.21 |  |
| B | -0.04 | Si | -0.03 |  |
|  |  | Si | -0.11 |  |
|  |  | Si | -0.07 |  |
|  |  | Si | 0.00 |  |
|  |  | Si | -0.42 |  |
|  |  | Si | 0.01 |  |
|  |  | Si | -0.04 |  |
|  |  | Si | -0.02 |  |

B3Si11

| Atom | μs | Atom | μs | Σμs |
| --- | --- | --- | --- | --- |
| B | -0.04 | Si | -0.03 | -1.00 |
| B | 0.01 | Si | -0.05 |  |
| B | 0.01 | Si | -0.06 |  |
|  |  | Si | -0.29 |  |
|  |  | Si | -0.06 |  |
|  |  | Si | -0.07 |  |
|  |  | Si | -0.03 |  |
|  |  | Si | -0.05 |  |
|  |  | Si | -0.05 |  |
|  |  | Si | -0.29 |  |
|  |  | Si | 0.00 |  |

B3Si12

| Atom | μs | Atom | μs | Σμs |
| --- | --- | --- | --- | --- |
| B | 0.00 | Si | -0.01 | -1.00 |
| B | 0.00 | Si | -0.06 |  |
| B | 0.00 | Si | -0.05 |  |
|  |  | Si | -0.06 |  |
|  |  | Si | -0.01 |  |
|  |  | Si | -0.02 |  |
|  |  | Si | -0.07 |  |
|  |  | Si | -0.02 |  |
|  |  | Si | 0.00 |  |
|  |  | Si | -0.02 |  |
|  |  | Si | -0.07 |  |
|  |  | Si | -0.62 |  |

B3Si13

| Atom | μs | Atom | μs | Σμs |
| --- | --- | --- | --- | --- |
| B | -0.02 | Si | -0.01 | -1.00 |
| B | 0.00 | Si | -0.02 |  |
| B | 0.01 | Si | -0.08 |  |
|  |  | Si | -0.06 |  |
|  |  | Si | 0.01 |  |
|  |  | Si | -0.07 |  |
|  |  | Si | -0.02 |  |
|  |  | Si | -0.01 |  |
|  |  | Si | -0.06 |  |
|  |  | Si | 0.00 |  |
|  |  | Si | -0.03 |  |
|  |  | Si | -0.01 |  |
|  |  | Si | -0.63 |  |

B3Si14

| Atom | μs | Atom | μs | Σμs |
| --- | --- | --- | --- | --- |
| B | 0.02 | Si | 0.00 | -1.00 |
| B | -0.05 | Si | -0.07 |  |
| B | 0.02 | Si | -0.07 |  |
|  |  | Si | -0.06 |  |
|  |  | Si | -0.05 |  |
|  |  | Si | -0.05 |  |
|  |  | Si | -0.02 |  |
|  |  | Si | -0.05 |  |
|  |  | Si | -0.19 |  |
|  |  | Si | -0.07 |  |
|  |  | Si | -0.06 |  |
|  |  | Si | -0.10 |  |
|  |  | Si | -0.19 |  |
|  |  | Si | -0.02 |  |

B3Si15

| Atom | μs | Atom | μs | Σμs |
| --- | --- | --- | --- | --- |
| B | -0.01 | Si | -0.02 | -1.00 |
| B | -0.01 | Si | -0.04 |  |
| B | 0.02 | Si | -0.05 |  |
|  |  | Si | -0.07 |  |
|  |  | Si | -0.04 |  |
|  |  | Si | -0.02 |  |
|  |  | Si | -0.08 |  |
|  |  | Si | -0.12 |  |
|  |  | Si | -0.02 |  |
|  |  | Si | -0.04 |  |
|  |  | Si | -0.20 |  |
|  |  | Si | -0.08 |  |
|  |  | Si | -0.17 |  |
|  |  | Si | -0.01 |  |
|  |  | Si | -0.05 |  |

B3Si16

| Atom | μs | Atom | μs | Σμs |
| --- | --- | --- | --- | --- |
| B | -0.09 | Si | 0.00 | -1.00 |
| B | -0.06 | Si | 0.00 |  |
| B | -0.07 | Si | -0.03 |  |
|  |  | Si | -0.01 |  |
|  |  | Si | -0.02 |  |
|  |  | Si | -0.06 |  |
|  |  | Si | -0.05 |  |
|  |  | Si | -0.03 |  |
|  |  | Si | -0.01 |  |
|  |  | Si | -0.20 |  |
|  |  | Si | -0.03 |  |
|  |  | Si | -0.02 |  |
|  |  | Si | -0.23 |  |
|  |  | Si | -0.04 |  |
|  |  | Si | 0.00 |  |
|  |  | Si | -0.05 |  |

B3Si17

| Atom | μs | Atom | μs | Σμs |
| --- | --- | --- | --- | --- |
| B | 0.00 | Si | -0.03 | -1.00 |
| B | -0.01 | Si | -0.01 |  |
| B | 0.00 | Si | -0.06 |  |
|  |  | Si | 0.00 |  |
|  |  | Si | -0.02 |  |
|  |  | Si | -0.03 |  |
|  |  | Si | -0.03 |  |
|  |  | Si | 0.00 |  |
|  |  | Si | -0.02 |  |
|  |  | Si | 0.00 |  |
|  |  | Si | -0.02 |  |
|  |  | Si | -0.01 |  |
|  |  | Si | 0.00 |  |
|  |  | Si | -0.02 |  |
|  |  | Si | -0.68 |  |
|  |  | Si | -0.02 |  |
|  |  | Si | -0.02 |  |

# Footnotes

(Correspondence to:Yan-Fei Hu, School of Physics and Electronic Engineering, Sichuan University of Science ＆ Engineering, Zigong 643000, China. E-mail address: yanfei_hu1982@suse.edu.cn