Supporting file

A facile method for precipitating of dispersed carbon particles prepared by microwave heating and its application for dye removal

Fatemeh Seifikara, Saeid Aziziana,(

a Department of Physical Chemistry, Faculty of Chemistry, Bu-Ali Sina University, Hamedan, Iran

| RMS | R2 | α | n | b | a | F2 | k2 (g/mg.s) | k1 (1/s) | k | qe (mg/g) | Kinetics model |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0.2279 | 0.9990 | - | - | - | - | - | - | 0.29 | - | 16.48 | PFO |
| 0.6142 | 0.9929 | - | - | - | - | - | 0.02 | - | - | 18.63 | PSO |
| 0.2629 | 0.9990 | - | - | - | - | 0.03 | - | 0.28 | - | 16.49 | MOE |
| 1.0359 | 0.9800 | - | - | 0.32 | 31.80 | - | - | - | - | - | Elovich |
| 0.2819 | 0.9988 | 2.04 | - | - | - | - | - | - | 8.0×10-3 | 16.66 | FL-PSO |
| 0.2630 | 0.9990 | 0.99 | - | - | - | - | - | - | 29×10-3 | 16.49 | FL-PFO |

| RMS | R2 | α | n | b | a | F2 | k2 (g/mg.s) | k1 (1/s) | k | qe (mg/g) | Kinetics model |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0.1115 | 0.9999 | - | - | - | - | - | - | 0.43 | - | 22.78 | PFO |
| 0.7438 | 0.9957 | - | - | - | - | - | 0.03 | - | - | 24.53 | PSO |
| 0.0485 | 0.9999 | - | - | - | - | -1.03 | - | 0.61 | - | 22.73 | MOE |
| 1.2859 | 0.9871 | - | - | 0.34 | 332.27 | - | - | - | - | - | Elovich |
| 0.0450 | 0.9999 | 3.60 | - | - | - | - | - | - | 2.1×10-3 | 22.74 | FL-PSO |
| 0.0486 | 0.9999 | 1.20 | - | - | - | - | - | - | 34×10-3 | 22.73 | FL-PFO |

| RMS | R2 | α | n | b | a | F2 | k2 (g/mg.s) | k1 (1/s) | k | qe (mg/g) | Kinetic smodel |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0.6236 | 0.9953 | - | - | - | - | - | - | 0.29 | - | 20.49 | PFO |
| 0.7496 | 0.9932 | - | - | - | - | - | 0.02 | - | - | 22.63 | PSO |
| 0.7192 | 0.9953 | - | - | - | - | -0.15 | - | 0.31 | - | 20.46 | MOE |
| 1.0695 | 0.9863 | - | - | 0.31 | 75.20 | - | - | - | - | - | Elovich |
| 0.6764 | 0.9959 | 2.05 | - | - | - | - | - | - | 5.8×10-3 | 20.75 | FL-PSO |
| 0.7197 | 0.9953 | 1.03 | - | - | - | - | - | - | 28×10-3 | 20.47 | FL-PFO |

| RMS | R2 | α | n | b | a | F2 | k2 (g/mg.s) | k1 (1/s) | k | qe (mg/g) | Kinetics model |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1.2574 | 0.9942 | - | - | - | - | - | - | 0.23 | - | 37.20 | PFO |
| 2.3271 | 0.9802 | - | - | - | - | - | 7.1×10-3 | - | - | 42.06 | PSO |
| 0.5226 | 0.9992 | - | - | - | - | -2.67 | - | 0.48 | - | 36.60 | MOE |
| 3.5044 | 0.9552 | - | - | 0.13 | 39.15 | - | - | - | - | - | Elovich |
| 0.1060 | 0.9999 | 2.28 | - | - | - | - | - | - | 1.8×10-3 | 37.14 | FL-PSO |
| 0.5529 | 0.9991 | 1.45 | - | - | - | - | - | - | 13×10-3 | 36.60 | FL-PFO |

| R2 | n | KMLF | KML | qm (mg/g) | Isotherm Model |
| --- | --- | --- | --- | --- | --- |
| 0.9746 0.9870 | - 0.68 | - 54 | 58 - | 38.45 41.40 | ML MLF |

| R2 | n | KMLF | KML | qm (mg/g) | Isotherm Model |
| --- | --- | --- | --- | --- | --- |
| 0.9697 0.9838 | - 1.90 | - 10746 | 10257 - | 47.39 45.00 | ML MLF |

# Footnotes

( Corresponding author. Tel.: +98 813 8282807; Fax: +98 813 8257404.

E-mail address: sazizian@basu.ac.ir (S. Azizian).

# Text boxes

Intensity

Binding energy (k eV)

Fig. S1.  The EDS spectra of the prepared carbon particles.

Fig. S2. The XRD pattern of the prepared carbon.

Fig. S3. Diagram of ∆pH versus pHi of the prepared carbon.

pHPZC

(a)

Fig. S4. (a) FT-IR and (b) ATR-IR spectra of the prepared carbon.

(b)

Table S1. Obtained kinetic model parameters for the adsorption of methyl violet onto the prepared carbon (at 10 mg/l concentration).

Table S2. Obtained kinetic model parameters for the adsorption of methyl violet onto the prepared carbon (at 30 mg/l concentration).

Table S3. Obtained kinetic model parameters for the adsorption of cationic blue onto the prepared carbon (at 10 mg/l concentration).

Table S4. Obtained kinetic model parameters for the adsorption of cationic blue onto the prepared carbon (at 30 mg/l concentration).

Table S5. Obtained isotherm model parameters for the adsorption of cationic blue onto the prepared carbon.

Table S6. Obtained isotherm model parameters for the adsorption of methyl violet onto the prepared carbon.