A novel poly(ethyleneoxide)-based magnetic nanocomposite catalyst for highly efficient multicomponent synthesis of pyran derivatives Ali Maleki,a,* Mojtaba Azizia,b and Zeynab Emdadia aCatalysts and Organic Synthesis Research Laboratory, Department of Chemistry, Iran University of Science and Technology, Tehran 16846-13114, Iran bDepartment of Chemistry, K.N. Toosi University of Technology, P.O. Box 15875-4416, Tehran, Iran *Corresponding author. Tel.: +98 21 77240640-50; Fax: +98 21 73021584. E-mail: maleki@iust.ac.ir (Ali Maleki). Table of contents Subject Page Characterization of the selected product(4g) FT-IR spectrum of compound 4g (Figure S1)…………………………………… S2 1H NMR spectra of selected compounds (Figure S2-S4)……………….……….. S3-S10

Spectral data of the selected products

5-Ethoxycarbonyl-2-amino-4-(3-nitrophenyl)-3-cyano-6-methyl-4H-pyran; IR (KBr) (υmax, cm−1): 3402, 3326, 3080, 2987, 2925, 2191, 1691, 1674, 1647, 1604, 1529, 1344, 1267, 1062, 1000; 1HNMR (500 MHz, DMSO-d6): 1.023 (t, 3H, CH3, J = 6.9 Hz), 2.35 (s, 3H, CH3), 3.95-3.98 (m, 2H, CH2), 4.52 (s, 1H, CH), 7.08 (s, 1H, NH2), 7.62-7.66 (m, 2H, Ar), 7.98 (s, 1H, Ar), 8.11 (d,1H , Ar, J = 6.8 Hz).

Figure S1.  FT-IR spectrum of compound (4g) 3-Nitro-4H-pyran

Figure S2. 1H NMR spectrum of compound (4g) 3-Nitro-4H-pyran

Figure S3. 1H NMR spectrum of compound (4g) 3-Nitro-4H-pyran

Figure S4. 1H NMR spectrum of compound (4g) 3-Nitro-4H-pyran

Figure S5. 1H NMR spectrum of compound (4g) 3-Nitro-4H-pyran

Figure S6. 1H NMR spectrum of compound (4d)

Figure S7. 1H NMR spectrum of compound (4d)

Figure S8. 1H NMR spectrum of compound (4l)

Figure S9. 1H NMR spectrum of compound (4l)