Supporting Information

A new stable porous Pr-organic framework constructed by multi-iodine-substituted aromatic polycarboxylates: Synthesis, characterization and selective adsorption of dyes

YING SUN, FENG YING BAI, XUE MIN WANG, YU WANG, LI XIAN SUN and YONG HENG XING*

Supplementary Index

1. IR spectra	S3

2. UV-Vis spectra	S4

3. PXRD spectra	S5

4. TGA spectra	S6

5. Structure of compound 1	S7

6. UV-Vis calibration curves for organic dyes	S8

7. Atomic force microscope scan test	S11

8. EDX test	S13

9. Label thermal ellipsoid	S14

1. IR spectra

(a)

(b)

Figure S1. (a) The IR spectrum of ligand of H3TIBTC. (b) The IR spectrum of ligand of compound 1.

2. UV-Vis spectra

(a)

(b)

Figure S2. (a) The UV spectrum of ligand of H3TIBTC. (b) The UV spectrum of ligand of compound 1.

3. PXRD spectra

Figure S3. PXRD of compound 1.

4. TGA spectra

Figure S4. TG of compound 1.

5. Structure of compound 1

(a)

(b)

(c)

Figure S5. (a) The pore structure of compound 1. (b) PrO9 three cap triangular prismatic space configuration. (c) Simplified topology structure.

6. UV-Vis calibration curves for organic dyes

(a)

(b)

(c)

(d)

(e)

(f)

Figure S6. UV-Vis calibration curves for dyes: (a) eosin; (b) MG; (c) OG; (d) CBB R-250; (e) MB; (f) crystal violet.

7. Atomic force microscope scan test

(a)

(b)

(c)

Figure S7. (a) A perspective view of an unadsorbed dye solution. (b) A perspective view of a portion of the dye adsorbed. (c) A perspective view of the adsorbed dye after three cycles.

8. EDX test

(a)

(b)

Figure S8. (a) EDX diagram before adsorption. (b) Adsorbed EDX diagram.

9. Label thermal ellipsoid

Figure S9. A label thermal ellipsoid plot of the asymmetric unit of 1.

# Text boxes

10.07Å

17.43Å