Syntheses, structural diversity and properties of three coordination polymers built by chlorophenyl imidazole dicarboxylate

Zhifang Yue,a Feng Wang,a,b Xianqiang Li,a Zhenna Chen,a Yanyan Zhua, Gang Lia[[1]](#footnote-1)\*

Supporting Information

**Table S1.** Hydrogen bonds distances (Å) and angles (deg) for **1**- **3.**

|  |  |  |  |
| --- | --- | --- | --- |
| D-H...A | d(H...A) | d(D...A) | ∠(DHA) |
| **1** | | | |
| O(5)-H(5A)... N(1)#3 | 2.08 | 2.819(7) | 150.7 |
| **2** | | | |
| O(1)-H(1) ...O(9) | 1.72 | 2.552(3) | 177.2 |
| O(13)-H(14)...O(5) | 1.65 | 2.476(3) | 178.5 |
| O(15)-H(16) ...O(12)#3 | 1.86(7) | 2.672(4) | 176.2(5) |
| O(15)-H(15) ...O(4)#3 | 2.46(4) | 2.787(4) | 111(4) |
| **3** | | | |
| O(3)-H(3)...O(19)#3 | 1.90 | 2.680(5) | 159.2 |
| O(9)-H(9)...O(21) | 1.87 | 2.676(5) | 168.7 |
| O(12)-H(12)...O(20) | 1.87 | 2.680(5) | 167.4 |
| O(17)-H(107) ...O(11) | 1.904(18) | 2.734(5) | 162(5) |
| O(17)-H(107) ...O(7) | 2.51(4) | 3.028(4) | 119(4) |
| O(16)-H(101) ...Cl(2)#3 | 2.62(5) | 3.245(4) | 130(5) |
| O(16)-H(101) ...Cl(3)#5 | 2.86(5) | 3.441(4) | 126(5) |
| O(18)-H(103) ...O(15) | 1.91(2) | 2.737(5) | 160(6) |
| O(18)-H(103) ...O(2) | 2.61(5) | 3.017(5) | 111(4) |
| O(18)-H(104) ...Cl(1) | 2.70(6) | 3.243(4) | 122(5) |
| O(18)-H(104) ...Cl(1)#7 | 2.86(4) | 3.442(4) | 127(4) |
| O(19)-H(106) ...O(10)#8 | 2.09(3) | 2.866(5) | 150(6) |
| O(9)-H(114) ...O(8) | 1.92(7) | 2.755(4) | 163(6) |
| O(9)-H(114) ...O(7)  O(21)-H(113) ...O(18)#3 | 2.32(7)  2.09(4) | 2.960(4)  2.829(6) | 132(6)  143(6) |
| O(16)-H(115) ...O(5) | 1.92(2) | 2.734(4) | 158(5) |
| O(17)-H(116) ...N(6) | 2.05(3) | 2.862(5) | 156(5) |
| O(17)-H(116) ...O(7) | 2.51(4) | 3.028(4) | 119(4) |
| O(3)-H(118) ...O(13)#3 | 1.96(7) | 2.767(4) | 173(7) |
| O(3)-H(118) ...O(4) | 2.51(7) | 2.949(4) | 115(6) |
| O(20)-H(150) ...O(16) | 2.09(3) | 2.833(5) | 145(5) |
| O(20)-H(151) ...O(6)#8 | 2.07(3) | 2.858(5) | 153(6) |
| O(21)-H(153) ...O(14) | 2.10(6) | 2.862(5) | 147(10) |

Symmetry transformations used to generate equivalent atoms: For **1**: #3: -x+1, -y, -z+1. For **2**: #3: x-1, y, z. For **3**: #3: x, y, z-1; #5: x+1/2, -y+1/2, z+1/2; #7: x, -y, z+1/2; #8: x, y, z+1.

**Table S2**. Selected bond distances (Å) and angles (deg) for **1-3**

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| **1** | | | | | |
| Sr(1)-O(2)#1 | 2.488(4) | Sr(1)-O(5) | 2.733(5) | Sr(1)-O(1)#2 | 2.542(4) |
| Sr(1)-O(4)#4 | 2.779(4) | Sr(1)-O(1) | 2.697(4) | Sr(1)-O(4) #1 | 2.545(4) |
| Sr(1)-O(3) #4 | 2.710(4) | Sr(1)-O(3)#3 | 2.676(4) | Sr(1)-O(2) | 2.734(4) |
| O(2)#1-Sr(1)-O(1)#2 | 157.18(14) | O(3)#1-Sr(1)-O(2) | 70.49(12) | O(2)#1-Sr(1)-O(4) #1 | 70.48(14) |
| O(1)-Sr(1)-O(2) | 48.47(12) | O(1)#2-Sr(1)-O(4) #1 | 97.37(13) | O(3) #4-Sr(1)-O(2) | 61.61(12) |
| O(2)#1-Sr(1)-O(3)#3 | 65.24(14) | O(1)#2-Sr(1)-O(5) | 68.52(13) | O(1)#2-Sr(1)-O(3)#1 | 105.36(12) |
| O(4) #1-Sr(1)-O(5) | 69.28(14) | O(4)-Sr(1)-O(3)#3 | 114.53(13) | O(3)#3-Sr(1)-O(5) | 64.31(13) |
| O(2)#1-Sr(1)-O(1) | 75.49(13) | O(1)-Sr(1)-O(5) | 131.64(13) | O(1)#2-Sr(1)-O(1) | 121.68(10) |
| O(3) #4-Sr(1)-O(5) | 137.72(12) | O(4) #1-Sr(1)-O(1) | 139.60(13) | O(5)-Sr(1)-O(2) | 108.33(14) |
| O(3)#3-Sr(1)-O(1) | 67.60(12) | O(2)#1-Sr(1)-O(4)#4 | 109.85(14) | O(2)#1-Sr(1)-O(3) #4 | 132.98(14) |
| O(1)#2-Sr(1)-O(4)#4 | 81.14(13) | O(1)#2-Sr(1)-O(3) #4 | 69.29(13) | O(4) #1-Sr(1)-O(4)#4 | 66.95(15) |
| O(4) #1-Sr(1)-O(3) #4 | 113.97(13) | O(3)#3-Sr(1)-O(4)#4 | 172.78(13) | O(2)#1-Sr(1)-O(5) | 88.89(14) |
| O(3)#3-Sr(1)-O(3) #4  O(1)-Sr(1)-O(3) #4  O(2)#1-Sr(1)-O(2) | 131.48(6)  75.12(12)  118.31(11) | O(1)-Sr(1)-O(4)#4  O(3) #4-Sr(1)-O(4)#4  O(2)-Sr(1)-O(4)#4 | 106.47(13)  47.44(12)  109.05(13) | O(4) #1-Sr(1)-O(2)  O(5)-Sr(1)-O(4)#4  O(1)#2-Sr(1)-O(2) | 171.13(12)  121.86(13)  73.97(12) |
| **2** | | | | | |
| Cd(2)-N(2) | 2.326(2) | Cd(2)-N(1)#2 | 2.237(2) | Cd(1)-N(6) | 2.271(2) |
| Cd(2)-O(3) | 2.275(2) | Cd(1)-O(9) | 2.398(2) | Cd(2)-O(15) | 2.285(3) |
| Cd(2)-O(4)#2 | 2.504(2) | Cd(2)-O(4)#3 | 2.3060(19) | Cd(1)-O(12) | 2.401(2) |
| N(6)#1-Cd(1)-N(6) | 180.00(8) | N(1)#2-Cd(2)-O(3) | 108.87(8) | N(6)#1-Cd(1)-O(9) | 91.55(8) |
| N(1)#2-Cd(2)-O(15) | 99.54(9) | N(6)-Cd(1)-O(9) | 88.45(8) | O(3)-Cd(2)-O(15) | 151.50(9) |
| N(2)-Cd(2)-O(4)#2 | 175.24(7) | N(1)#2-Cd(2)-O(4)#3 | 140.62(8) | O(9)-Cd(1)-O(9)#1 | 180.000(1) |
| O(3)-Cd(2)-O(4)#3  N(6)-Cd(1)-O(12)  O(3)-Cd(2)-N(2)  O(12)-Cd(1)-O(12)#1  N(1)#2-Cd(2)-O(4)#2 | 81.69(8)  72.62(7)  74.14(8)  180.0  69.71(7) | N(6)#1-Cd(1)-O(12)  N(1)#2-Cd(2)-N(2)  O(9)#1-Cd(1)-O(12)  O(4)#3-Cd(2)-N(2)  O(15)-Cd(2)-O(4)#2 | 107.38(7)  105.86(9)  104.71(8)  113.50(8)  78.71(9) | O(15)-Cd(2)-O(4)#3  O(9)-Cd(1)-O(12)  O(15)-Cd(2)-N(2)  O(4)#3-Cd(2)-O(4)#2  O(3)-Cd(2)-O(4)#2 | 74.75(9)  75.29(8)  100.67(9)  70.97(8)  108.67(7) |
| **3** | | | | | |
| Co(1)-O(1) | 2.070(3) | Co(2)-O(6) | 2.102(3) | Co(1)-O(11) | 2.075(3) |
| Co(2)-O(4) | 2.156(3) | Co(1)-O(9) | 2.076(3) | Co(2)-N(2) | 2.223(3) |
| Co(1)-O(10)  Co(3)-O(15)  Co(2)-O(5)  Co(3)-O(2) | 2.098(3)  2.067(3)  2.065(3)  2.163(3) | Co(3)-O(13)  Co(1)-N(5)  Co(3)-O(14)  Co(2)-O(8) | 2.063(3)  2.226(4)  2.103(3)  2.072(3) | Co(1)-O(7)  Co(3)-O(12)  Co(2)-O(3)  Co(3)-N(3) | 2.163(3)  2.077(3)  2.066(3)  2.223(3) |
| O(1)-Co(1)-O(11) | 90.53(12) | O(3)-Co(2)-O(4) | 88.58(12) | O(1)-Co(1)-O(9) | 91.26(12) |
| O(8)-Co(2)-O(4) | 83.55(11) | O(11)-Co(1)-O(9) | 174.23(13) | O(6)-Co(2)-O(4) | 94.45(11) |
| O(1)-Co(1)-O(10) | 178.10(13) | O(5)-Co(2)-N(2) | 87.81(12) | O(11)-Co(1)-O(10) | 89.42(12) |
| O(3)-Co(2)-N(2) | 97.04(13) | O(9)-Co(1)-O(10) | 88.61(12) | O(8)-Co(2)-N(2) | 104.99(12) |
| O(1)-Co(1)-O(7) | 83.86(12) | O(6)-Co(2)-N(2) | 77.02(12) |  |  |

Symmetry transformations used to generate equivalent atoms. For **1**: #1: -x+1, y+1/2, -z+1/2; #2: -x+1, y-1/2, -z+1/2; #3: -x+1, -y, -z+1; #4: x, -y-1/2, z-1/2; #5: x, -y-1/2, z+1/2. For **2**: #1: -x+1, -y, -z+2; #2: -x+1, -y+1, -z+2; #3: x-1, y, z; #4: x+1, y, z. For **3**: #1: x-1/2, -y+1/2, z-1/2; #2: x+1/2, -y+1/2, z-1/2; #3: x, y, z-1; #4: x, -y, z-1/2; #5: x+1/2, -y+1/2, z+1/2; #6: x-1/2, -y+1/2, z+1/2; #7: x, -y, z+1/2; #8: x, y, z+1.




Figure S1a PXRD pattern of compound **1** at room temperature




Figure S1b PXRD pattern of compound **2** at room temperature




Figure S1c PXRD pattern of compound **3** at room temperature

1. \* Corresponding author. *Email address*: [gangli@zzu.edu.cn](mailto:gangli@zzu.edu.cn) (G. Li). [↑](#footnote-ref-1)