Supplementary Information

for

The removal of Pb (II) and Cd (II) with hydrous manganese dioxide: Mechanism on zeta potential and adsorption behavior

Shanshan Wua, Fencun Xie a*

School of Chemistry and Chemical Engineering, South China University of Technology, Guangzhou, 510641, P. R. China

Corresponding author:

Fencun Xiea*

School of Chemistry and Chemical Engineering, South China University of Technology, Guangzhou, 510641, P. R. China

E-mail: acfchxie@scut.edu.cn

Table 1. The number of HMO with different ZP values

|  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| MnO4-/Mn2+ | 1:1 | 1:1.1 | 1:1.2 | 1:1.3 | 1:1.4 | 1:1.5 | 1:1.6 | 1:1.7 | 1:1.8 | 1:1.9 | 1:2 |
| ZP value(mV) | -51.7 | -49.0 | -44.6 | -42.2 | -40.8 | -38.6 | -35.4 | -32.6 | -29.6 | -26.3 | -21.8 |

Table 2. The BET analysis of HMOs

|  | 1-HMO | 3-HMO | 5-HMO | 7-HMO | 9-HMO | 11-HMO |
| --- | --- | --- | --- | --- | --- | --- |
| Zeta potential(mV) | -51.7 | -44.6 | -40.8 | -35.4 | -29.6 | -21.8 |
| Surface area(m2/g) | 66.88 | 64.80 | 62.00 | 60.00 | 59.00 | 58.21 |
| Average pore size(nm) | 5.39 | 7.20 | 7.55 | 8.28 | 12.10 | 15.53 |

Table 3 The parameter of linear function for Pb (II) and Cd (II)

|  | Slope | Intercept | R2 |
| --- | --- | --- | --- |
| Pb (II) | -7.68 | 75.12 | 0.99 |
| Cd (II) | -2.65 | 0.29 | 0.99 |

Table 4 The parameters of Langmuir and Freundlich isotherm model

| heavy metal | Temperature/K | Langmuir |  |  |  | Freundlich |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Qm (mg/g) | KL | R2 |  | KF | 1/n | R2 |
| Pb | 293.15 | 469.1 | 4.3 | 0.99 |  | 365.6 | 0.06 | 0.90 |
|  | 303.15 | 475.4 | 131.1 | 0.97 |  | 416.4 | 0.05 | 0.66 |
|  | 313.15 | 487.0 | 118.7 | 0.99 |  | 435.7 | 0.04 | 0.64 |
| Cd | 293.15 | 128.2 | 20.5 | 0.99 |  | 115.1 | 0.05 | 0.79 |
|  | 303.15 | 140.3 | 6.2 | 0.98 |  | 117.0 | 0.06 | 0.92 |
|  | 313.15 | 154.6 | 3.9 | 0.99 |  | 120.2 | 0.06 | 0.94 |

Table 5 The comparison of the Langmuir maximum adsorption capacity onto various adsorbents for Pb (II) and Cd (II)

| Heavy metal ion | Adsorbents | qm (mg/g) | Refs. |
| --- | --- | --- | --- |
| Pb (II) | chitosan functionalized magnetic nanoparticles | 498.6 | [1] |
|  | HMO | 475.4 | This study |
|  | sulphuric acid-treated cashew nut shell | 408.6 | [2] |
|  | surface modified Strychnos potatorum seeds | 166.7 | [3] |
|  | β-MnO2 | 13.6 | [4] |
| Cd (II) | MnO2 nanosheet | 348 | [5] |
|  | freshly synthesized hydrous manganese dioxide | 168.4 | [6] |
|  | HMO | 140.3 | This study |
|  | polying alcohol/polyacrylic acid double network gel | 115.9 | [7] |
|  | Surface modified Eucalyptus seeds | 71.2 | [8] |

Table 6 Thermodynamic parameters for the adsorption of Pb (II) and Cd (II)

|  | Initial con. (mg/L) | ΔH (kJ/mol) | ΔS (J/mol/K) | ΔG (kJ/mol) |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | 293.15 | 303.15 | 313.15 |
| Pb | 90 | 164.4 | 596.2 | -10.6 | -16.6 | -22.5 |
|  | 100 | 61.3 | 239.8 | -9.3 | -11.7 | -14.1 |
|  | 110 | 24.2 | 107.9 | -7.6 | -8.7 | -9.8 |
| Cd | 20 | 28.8 | 149.7 | -15.1 | -16.6 | -18.1 |
|  | 30 | 9.5 | 60.7 | -8.3 | -8.9 | -9.5 |
|  | 40 | 5.0 | 35.8 | -5.5 | -5.8 | -6.2 |

Table 7 The kinetic model constants and correlation coefficients for Pb (II)

|  |  | pseudo-first order model |  |  | pseudo-second order model |  |  | intraparticle diffusion model |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | qe(mg/g) | k1(s-1) | R2 | qe(mg/g) | k2(g/mg*s) | R2 | kp(mg/g min1/2) | C | R2 |
| Pb | 1-HMO | 465.7 | 0.22 | 0.83 | 467.3 | 0.0069 | 0.99 | 12.06 | 405.7 | 0.95 |
|  | 3-HMO | 419.7 | 0.39 | 0.82 | 421.9 | 0.0056 | 0.99 | 21.19 | 321.1 | 0.74 |
| Cd | 1-HMO | 135.3 | 0.12 | 0.90 | 135.9 | 0.0201 | 0.99 | 2.02 | 122.4 | 0.85 |
|  | 3-HMO | 123.7 | 0.20 | 0.73 | 124.5 | 0.0135 | 0.99 | 3.86 | 100.1 | 0.58 |

Fig. 1 The relationship between ZP value and ratio of KMnO4 and MnSO4

Fig. 2 The XRD spectrum of HMOs with different Zeta potential

Fig. 3 The SEM images of 1-HMO (a), 6-HMO (b) and 11-HMO (c) and TEM images of 1-HMO (d) and 11-HMO (e)

Fig. 4 The correlation between zeta potential and adsorption capacity (a) and removal rate (b)

Fig. 5 Effect of pH on Pb (II) and Cd (II) removal by 1-HMO

Fig. 6 Isotherm adsorption of Pb (II) and Cd (II) on 1-HMO in (a-d)

Fig. 7 Thermodynamic study

Fig. 8 The kinetic study of Pb (II) and Cd (II) on 1 and 3-HMO

Fig. 9 Intraparticle diffusion model

Fig. 10 SEM-EDS spectra of HMO nanoparticles before and after adsorbing Pb (II) and Cd (II)

Fig. 11 The FT-IR spectrum of 1-HMO adsorbent before and after adsorbing Pb (II) and Cd (II)

Fig. 12 The XPS full spectrum of 1-HMO before and after adsorption of Pb (II) and Cd (II) (a); O (1s) spectra before adsorption (b) and after adsorption of Pb (II) (c); Pb (4f) spectra (d) and Cd (3d) spectra of 1-HMO after adsorption

Fig. 13 the removal efficiency of heavy metal ion and ZP value versus recycle times of HMO

# References

1.	Christopher FC, Anbalagan S, Kumar PS, Pannerselvam SR, Vaidyanathan VK: Surface adsorption of poisonous Pb(II) ions from water using chitosan functionalised magnetic nanoparticles. Iet Nanobiotechnol 2017, 11(4):433-442.

2.	Kumar PS, Ramalingam S, Abhinaya RV, Thiruvengadaravi KV, Baskaralingam P, Sivanesan S: Lead(II) Adsorption onto Sulphuric Acid Treated Cashew Nut Shell. Sep. Sci. Technol.2011, 46(15):2436-2449.

3.	Senthil Kumar P, Senthamarai C, Sai Deepthi ASL, Bharani R: Adsorption isotherms, kinetics and mechanism of Pb(II) ions removal from aqueous solution using chemically modified agricultural waste. Canadian J. Chem. Eng. 2013, 91(12):1950-1956.

4.	Zhao D, Yang X, Zhang H, Chen C, Wang X: Effect of environmental conditions on Pb(II) adsorption on β-MnO2. Chem. Eng. J. 2010, 164(1):49-55.

5.	Peng L, Zeng Q, Tie B, Lei M, Yang J, Luo S, Song Z: Manganese Dioxide nanosheet suspension: A novel absorbent for Cadmium(II) contamination in waterbody. J. Colloid. Interf. Sci. 2015, 456:108-115.

6.	Zhai Y, Wang H: Kinetics and mechanism study on adsorption of cadmium by freshly synthesized hydrous manganese dioxide. Desalin. Water Treat 2015, 57(15):6981-6990.

7.	Chu L, Liu C, Zhou G, Xu R, Tang Y, Zeng Z, Luo S: A double network gel as low cost and easy recycle adsorbent: Highly efficient removal of Cd(II) and Pb(II) pollutants from wastewater. J. Hazard. Mate. 2015, 300:153-160.

8.	Kiruba UP, Kumar PS, Prabhakaran C, Aditya V: Characteristics of thermodynamic, isotherm, kinetic, mechanism and design equations for the analysis of adsorption in Cd(II) ions-surface modified Eucalyptus seeds system. J. Taiwan Institute. Chem. Eng. 2014, 45(6):2957-2968.