Supplemental Data

Multiple Linear Regression Applied to Predicting Droplet Size of Complex Perfluorocarbon Nanoemulsions from Composition

Eric Lamberta and Jelena M. Janjic*,a,b

a Graduate School of Pharmaceutical Sciences, Duquesne University, 600 Forbes Avenue, Pittsburgh, PA 15282, USA; b Chronic Pain Research Consortium, Duquesne University, 600 Forbes Avenue, Pittsburgh, PA 15282, USA

Supp. Table 1. PFPE-tyramide solubility results by visual analysis. Scale bar reads 100 µm. Transcutol was selected as the carrier for PFPE-tyramide on the basis of appearance of each sample to the naked eye and appearance under 40x magnification.

| Excipient | No magnification | 40x magnification | Comment |
| --- | --- | --- | --- |
| Miglyol 812 |  |  | Large solid chunk visible at 1x; clear; very small amount visible under 40x; very low solubility |
| Olive oil |  |  | Large solid chunk visible at 1x; clear; small amount visible under 40x; low solubility |
| PFPE-oxide |  |  | Moderate solid chunk visible at 1x; translucent; considerable amount visible under 40x; low solubility |
| PCE |  |  | Small solid chunk visible at 1x; opaque; considerable amount visible under 40x; low solubility |
| CrEL |  |  | Large solid chunk visible at 1x; clear; small amount visible under 40x; low solubility |
| Transcutol |  |  | No solid chunk visible at 1x; clear to translucent; moderate amount visible under 40x; good solubility. Evidence of self-assembly |

Inclusion of process variables among mixture variables in multiple linear regression analysis introduces certain limitations in which a process main effect cannot be analyzed in the presence of mixture main effects; therefore a preliminary analysis of the data was conducted on: 1) the main effect of PFPE-tyramide in simple linear regression and 2) the PFPE-tyramide interactions in the presence of mixture main effects and interaction effects. Supp. Table 2 and Supp. Table 3 show that none of the PFPE-tyramide regression coefficients are statistically significant in these analyses, so they were omitted from the subsequent regression analysis.

Supp. Table 2. Regression coefficients for PFPE-tyramide in simple linear regression.

| Term | Estimate | Std Error | t Ratio | P-value |
| --- | --- | --- | --- | --- |
| Intercept | 144.17 | 2.94 | 49.12 | <.0001 |
| T | 1.58 | 5.08 | 0.31 | 0.759 |

Supp. Table 3. Regression coefficients for special cubic model.

| Term | Estimate | Std Error | t Ratio | P-value |
| --- | --- | --- | --- | --- |
| Intercept | 126.17 | 4.66 | 27.09 | <.0001 |
| A | 6.42 | 6.04 | 1.06 | 0.3233 |
| B | 29.95 | 6.04 | 4.96 | 0.0016 |
| C | 21.49 | 6.04 | 3.56 | 0.0093 |
| D | 49.05 | 6.04 | 8.11 | <.0001 |
| AC | -41.43 | 14.03 | -2.95 | 0.0214 |
| AD | -72.13 | 14.03 | -5.14 | 0.0013 |
| AT | 4.04 | 5.40 | 0.75 | 0.4782 |
| BC | -19.42 | 14.03 | -1.38 | 0.2089 |
| BD | -69.88 | 14.03 | -4.98 | 0.0016 |
| BT | -1.25 | 5.40 | -0.23 | 0.8234 |
| CT | 12.55 | 5.40 | 2.33 | 0.053 |
| DT | 3.61 | 5.40 | 0.67 | 0.5253 |
| ACT | 26.32 | 34.93 | 0.75 | 0.4757 |
| ADT | -51.68 | 34.93 | -1.48 | 0.1826 |
| BCT | 26.50 | 34.93 | 0.76 | 0.4729 |
| BDT | 41.72 | 34.93 | 1.19 | 0.2713 |

Z-average droplet size and zeta potential for all nanoemulsions were examined periodically using dynamic light scattering. Multiple representations of the measurements are included to demonstrate long-term stability in Supp. Figure 1, 2, 3, 4, 5, 6, and 7.

A

B

C

Supp. Figure 1. Nanoemulsions were stored at 4 °C and monitored for change in size over time to demonstrate shelf-life. Lines are put in place only to aid the reader.

A

B

C

Supp. Figure 2. Nanoemulsions were stored at 4 °C and monitored for change in PDI over time to demonstrate shelf-life. Lines are put in place only to aid the reader.

A

B

C

Supp. Figure 3. Nanoemulsions were stored at 4 °C and monitored for change in zeta potential over time to demonstrate shelf-life. Lines are put in place only to aid the reader.

Supp. Figure 4. Size distribution overlays for selected nanoemulsions. Solid lines represent measurements made within the first week of production. Dashed lines represent measurements made at a later follow up time (23 weeks post-production).

Supp. Figure 5. Zeta potential distribution overlays for selected nanoemulsions. Solid lines represent measurements made within the first week of production. Dashed lines represent measurements made at a later follow up time (23 weeks post-production).

Supp. Figure 6. Size distribution overlays for selected nanoemulsions. Solid lines represent measurements made within the first week of production. Dashed lines represent measurements made at a later follow up time (37, 53, and 53 weeks post-production for NEs 3, 17, and 18, respectively).

Supp. Figure 7. Zeta potential distribution overlays for selected nanoemulsions. Solid lines represent measurements made within the first week of production. Dashed lines represent measurements made at a later follow up time (37, 53, and 53 weeks post-production for NEs 3, 17, and 18, respectively).

Supp. Figure 8. Centrifugation conditions elicited very small responses for all two-phase nanoemulsions and consequently the test was abandoned for remainder of emulsions.