The side chain effects on TPD-based copolymers: the linear chain leads to a higher Jsc

Qiang Tao,*a,b Yafen Fu,a Qian Liu,a E’Zhou,a Dong Yan,a Zhengjun Fang,a,b Yunfeng Liao,a Xianwei Huang,a Jiyong Deng*a, and Donghong Yu*b,c

a Hunan Provincial Key Laboratory of Environmental Catalysis & Waste Recycling, School of Chemistry and Chemical Engineering, Hunan Institute of Engineering, Xiangtan 411104, China.

bDepartment of Chemistry and Bioscience, Aalborg University, DK-9220 Aalborg, Denmark

c Sino-Danish Center for Education and Research (SDC), DK-8000, Aarhus, Denmark

E-mails: qt@bio.aau.dk, djyong@yeah.net, yu@bio.aau.dk

Table S1 Photovoltaic parameters of PT1 and PT2-based polymer solar cells in an inverted device.

| polymer | Voc (V) | Jsc (mA/cm2) | FF | PCE (%) |
| --- | --- | --- | --- | --- |
| PT1 | 0.86 | 7.03 | 0.46 | 2.75 |
| PT2 | 0.91 | 3.93 | 0.51 | 1.83 |

Figure S1 J–V characteristics of PT1 and PT2 with an inverted device configuration of ITO/ZnO/Polymer:PC71BM/MoO3/Al.

Figure S2.1H NMR spectra of PT1 and PT2.