Supplementary-Tables

Table S-1 Properties of macroporous resins used in the study

| Resin | Framework | Polarity | Particle diameter (mm) | Surface area (m2/g) | Average pore diameter (nm) | Pore rate (%) | Pore volume (mL/g) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| HPD100 | Polythene | - | 0.3-1.20 | 650-700 | 85-90 |  |  |
| H103 |  | - | 0.3-1.25 | 1000-1100 | 85-95 | 55-59 | 1.08-1.12 |
| 001×1.1 |  | strong | 0.3-1.25 |  |  |  |  |
| D101 |  | weak | 0.25-0.84 | 500-550 | 90-100 |  |  |
| NKA-9 |  | strong | 0.3-1.25 | 250-290 | 155-165 | 46-50 |  |
| D151 |  | weak | 0.3-1.25 |  |  |  |  |

Tale S-2 Elution properties of different macroporous resins

| Type of Resin | Adsorption content（mg/g） | Desorption content（mg/g） | Elution (%) |
| --- | --- | --- | --- |
| D101 | 7.55 | 6.82 | 90.38 |
| HPD100 | 8.56 | 8.29 | 96.78 |
| NKA-9 | 8.40 | 8.24 | 98.14 |

Table S-3 Eluting of different macroporous resins

| The types of resins | Elution content（mg/g resin） |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | 10% | 30% | 50% | 70% | 90% |
| D101 | 1.8±0.02 | 4.3±0.14 | 1.3±0.08 | 0.3±0.01 | 0.2±0.01 |
| HPD100 | 1.5±0.02 | 3.4±0.14 | 2.1±0.08 | 0.6±0.01 | 0.1±0.01 |
| NKA-9 | 1.3±0.02 | 4.1±0.14 | 2.4±0.08 | 0.8±0.01 | 0.0±0.01 |

Supplementary-Figures

Figure S-1 total flavonoids, carotene, rutin, and the others contents of CL (mg·100g -1 dry weight)

FigureS-2 Flavonoid compounds adsorption capacities of macroporous resins used in the study

Figure S-3 Effect of different solvents on the extracting flavonoids from cassava leaves

Figure S-4 HPLC chromatogram of cassava leaves ethanol extracts and flavonoids standards

Figure S-5 HPLC/FTICR-MS chromatogram of cassava leaves flavonoids and rutin

Figure S-6 ESI-MS/MS2 chromatograms of compound 1(cloven)                         Figure S-6 Fragmentation scheme of compound 1(cloven)

Figure S-7 ESI-MS/MS2 chromatograms of compound 2 (myricetin-3-O-rutinoside)          Figure S-7 Fragmentation scheme of compound 2

Figure S-8 ESI-MS/MS2 chromatograms of compound 3 (robinin)                         Figure S-8 Fragmentation scheme of compound 3 (robinin)

Figure S-9 ESI-MS/MS2 chromatograms of compound 4 (rutin)                                  Figure S-9 Fragmentation scheme of compound 4 (rutin)

Figure S-10 ESI-MS/MS2 chromatograms of compound 5 (hyperoside)           Figure S-10 Fragmentation scheme of compound 5 (hyperoside)

Figure S-11 ESI-MS/MS2 chromatograms of compound 6 (nicotiflorin)             Figure S-11 Fragmentation scheme of compound 6 (nicotiflorin)

Figure S-12 ESI-MS/MS2 chromatograms of compound 7 (narcissin)                     Figure S-12 Fragmentation scheme of compound 7 (narcissin)