Supporting information for

Enhanced photovoltaic performances of C219-based dye sensitizers by introducing electron-withdrawing substituents: a density functional theory study

Caibin Zhaoa(, Qiang Zhanga, Xiaohu Yua*, Ke Zhoua, Lingxia Jina* and Wenliang Wangb

aShaanxi Key Laboratory of Catalysis, School of Chemical and Environmental Science, Shaanxi University of Technology, Hanzhong, Shaanxi 723001, P. R. China

bKey Laboratory for Macromolecular Science of Shaanxi Province, School of Chemistry and Chemical Engineering, Shaanxi Normal University, Xi’an, Shaanxi 710062, P. R. China

(Contents

Table S1 Calculated excited energies for the C219 dye with different TD-DFT methods

Figure S1 Simulated and experimental UV-vis absorption spectra for the C219 dye with the TD-CAM-B3LYP/6-31G(d) method

Table S2 Calculated frontier molecular orbital levels for the C219 dye with different DFT methods

Table S3 Calculated frontier molecular orbital levels for the C219 dye with the optimized CAM-B3LYP/6-31G(d) method

Table S4 Optimized main dihedral angles between adjacent units in all studied dyes with the B3LYP/6-31G(d) method

Figure S2 Optimized geometries for 1/(TiO2)38, 3/(TiO2)38, 5/(TiO2)38, and 7/(TiO2)38 complexes

Figure S3 Optimized slant angles for all studied dye/(TiO2)38 complexes

Table S5 Optimized Ti-O bond lengths for all studied dye/(TiO2)38 complexes

Table S6 Calculated hole-electron distances (Dhe) and hole-electron overlaps (Ohe) for all studied dyes in the S1 state

Figure S4 Calculated HOMO and LUMO profiles with Isovalue=0.04(left: HOMOs, right: LUMOs)

Figure S5 Schematic diagram of the distance from the HOMO/LUMO center to the TiO2 surface (d1 represents the distance from the HOMO center to the TiO2 surface, and d2 represents the distance from the LUMO center to the TiO2 surface)

description process of in cus equation

Calculation details of the relevant parameters in Marcus model

Table S1

| Functional/Basis | λmax/nm | Δλmax/nmb |
| --- | --- | --- |
| B3LYP/6-311G(d,p) | 646.7 | 153.7 |
| B3PW91/6-311G(d,p) | 645.2 | 152.2 |
| CAM-B3LYP/6-311G(d,p) | 497.7 | 4.7 |
| CAM-B3LYP/6-31G(d) | 494.6 | 1.6 |
| M062X/6-311G(d,p) | 499.7 | 6.7 |
| MPW1PW91/6-311G(d,p) | 750.8 | 257.8 |
| PBEPBE/6-311G(d,p) | 911.5 | 418.5 |
| TPSSTPSS/6-311G(d,p) | 883.3 | 390.3 |
| wB97XD/6-311G(d,p) | 480.8 | -12.2 |
| Exp.t | 493.0a | / |

a From the reference [12]. b Δλmax=λmax(Cal.)- λmax(Exp.)

Figure S1

Table S2

| Scheme | Calculated value | Deviation b |
| --- | --- | --- |
|  | EHOMO | ELUMO | Egap | △EHOMO | △ELUMO | △Egap |
| B3LYP/6-31G(d) | -4.875 | -2.765 | 2.110 | 0.085 | 0.705 | 0.62 |
| B3PW91/6-31G(d) | -4.816 | -2.904 | 1.912 | 0.144 | 0.566 | 0.422 |
| CAM-B3PW91/6-31G(d) | -5.830 | -1.840 | 3.990 | -0.870 | 1.630 | 2.500 |
| LC-wPBE/6-31G(d) | -7.034 | -1.167 | 5.867 | -2.074 | 2.303 | 4.377 |
| M062X/6-31G(d) | -5.833 | -2.204 | 3.629 | -0.873 | 1.266 | 2.139 |
| PBEPBE/6-31G(d) | -4.118 | -3.162 | 0.956 | 0.842 | 0.308 | -0.534 |
| MPW1PW91/6-31G(d) | -4.967 | -2.796 | 2.171 | -0.007 | 0.674 | 0.681 |
| TPSSTPSS/6-31G(d) | -4.109 | -3.110 | 0.999 | 0.851 | 6.58 | -0.491 |
| wb97XD/6-31G(d) | -6.413 | -1.357 | 5.056 | -1.453 | 2.113 | 3.566 |
| Experimental FMO levela | -4.960 | -3.470 | 1.490 |  |  |  |

a From reference [12].

b△EHOMO= EHOMO(Exp.)- EHOMO(Cal.), △ELUMO= ELUMO(Exp.)- ELUMO(Cal.), △Egap= Egap(Exp.)- Egap(Cal.).

Table S3

EXP=P2EXHF + P1(P4EXSlater + P3ΔExnon-local) + P6EClocal + P5ΔECnon-local

| Scheme | Calculated value | Deviation value b |
| --- | --- | --- |
|  | EHOMO | ELUMO | Egap | △EHOMO | △ELUMO | △Egap |
| 1 | -5.830 | -1.840 | 3.990 | 0.870 | -1.630 | -2.500 |
| 2 | -5.106 | -3.073 | 2.033 | 0.146 | -0.397 | -0.543 |
| 3 | -4.064 | -2.615 | 1.449 | -0.896 | -0.855 | 0.041 |
| 4 | -4.582 | -2.846 | 1.736 | -0.378 | -0.624 | -0.246 |
| 5 | -4.167 | -2.661 | 1.506 | -0.793 | -0.809 | -0.016 |
| 6 | -4.115 | -2.638 | 1.477 | -0.845 | -0.832 | 0.013 |
| 7 | -5.553 | -4.063 | 1.490 | 0.593 | 0.593 | 0.000 |
| 8 | -4.868 | -3.384 | 1.484 | -0.092 | -0.086 | 0.006 |
| 9 | -5.005 | -3.520 | 1.485 | 0.045 | 0.050 | 0.005 |
| 10 | -4.936 | -3.452 | 1.484 | -0.024 | -0.018 | 0.006 |
| Exp.a | -4.96 | -3.47 | 1.49 | / | / | / |

a From reference [12].

b△EHOMO= EHOMO(Exp.)- EHOMO(Cal.), △ELUMO= ELUMO(Exp.)- ELUMO(Cal.), △Egap= Egap(Exp.)- Egap(Cal.).

1. P1=1.00, P2=0.19, P3=0.65, P4=0.81, P5=0.65, P6=0.35.  2. P1=0.80, P2=0.40, P3=0.65, P4=0.81, P5=0.65, P6=3.45.

3. P1=0.80, P2=0.20, P3=0.65, P4=0.81, P5=0.65, P6=3.45.  4. P1=0.80, P2=0.30, P3=0.65, P4=0.81, P5=0.65, P6=3.45

5. P1=0.80, P2=0.22, P3=0.65, P4=0.81, P5=0.65, P6=3.45.  6. P1=0.80, P2=0.21, P3=0.65, P4=0.81, P5=0.65, P6=3.45.

7. P1=0.80, P2=0.21, P3=0.65, P4=0.81, P5=0.00, P6=4.50.  8. P1=0.80, P2=0.21, P3=0.65, P4=0.81, P5=0.00, P6=4.00.

9. P1=0.80, P2=0.21, P3=0.65, P4=0.81, P5=0.00, P6=4.10.  10. P1=0.80, P2=0.21, P3=0.65, P4=0.81, P5=0.00, P6=4.05.

Table S4

| Dye | I | II | III |
| --- | --- | --- | --- |
| C219 | 16.5 | 1.3 | 0.1 |
| 1 | 18.7 | 0.7 | 24.1 |
| 2 | 17.6 | 1.6 | 10.1 |
| 3 | 16.7 | 1.5 | 11.1 |
| 4 | 15.6 | 1.4 | 0.1 |
| 5 | 18.1 | 0.2 | 0.1 |
| 6 | 17.5 | 1.5 | 0.4 |
| 7 | 18.5 | 1.5 | 1.0 |

Figure S2

Figure S3

Table S5

| Dye | R1/Å | R2/Å |
| --- | --- | --- |
| C219 | 2.037 | 2.156 |
| 1 | 2.075 | 2.077 |
| 2 | 2.102 | 2.173 |
| 3 | 2.063 | 2.074 |
| 4 | 2.053 | 2.103 |
| 5 | 2.032 | 2.112 |
| 6 | 2.076 | 2.126 |
| 7 | 2.087 | 2.199 |

Table S6 Calculated hole-electron distances (Dhe) and hole-electron overlaps (Ohe) for all studied dyes in the S1 state

| Dye | Dhe/Å | Ohe/Å |
| --- | --- | --- |
| C219 | 3.184 | 0.418 |
| 1 | 3.578 | 0.383 |
| 2 | 3.913 | 0.369 |
| 3 | 3.787 | 0.379 |
| 4 | 4.374 | 0.353 |
| 5 | 3.416 | 0.403 |
| 6 | 3.783 | 0.376 |
| 7 | 3.390 | 0.400 |

Figure S4

Figure S5

Calculation details of the relevant parameters in Marcus model

1. Driving forces of the electron injection(ΔGinj) and electron recombination (ΔGrec)

According to the previous study, in DSSCs the ΔG in the electron injection (ΔGinj) and electron recombination (ΔGrec) processes can be estimated with [1],

(S1)

(S2)

where ECB is the conduction band energy level of TiO2, E*dye/Edye is the oxidation potential of excited/ground state, and E0-0 is the vertical transition energy.

2. Reorganization energy (λ)

As shown in Eq(8), the λ is the sum of structural relaxation from dye molecule (λdye), semiconductor (λsc), and organic solvent (λsol) in the electron transfer process,

(S3)

Generally, the λdye can be calculated with the classical adiabatic potential energy surface (PES) method [2]. According to the four-point model, the λdye term in the electron injection (λinj) and electron recombination (λrec) processes can be obtained with [3]

(S4)

(S5)

where E*(g*)/E*(g+) is the excited state energy with the excited state/cationic geometry, E+(g*)/E+(g+) is the cationic energy with the excited state/cationic geometry, E0(g+)/E0(g0) is the neutral energy with the cationic/neutral geometry, E+(g0)/E+(g+) is the cationic energy with the cationic/neutral geometry. On basis of the study from Wei et al, the λsc was set to 0.026eV [4]. Relatively, the λsol term is still not easy to be calculated accurately. Here, the λsol was approximately estimated with the modified Marcus scheme [5]. According to this model, the λsol is calculated by,

(S6)

(S7)

where/is the optical/static dielectric constant of solvent, which is 1.81/37.50 for acetonitrile, / is the optical/static (6.45/48.00) dielectric constant of TiO2, rA is the dye radius, and d is the distance between the TiO2 surface and the dye LUMO/HOMO center for the electron injection/recombination process.

3. Electron coupling (V)

According to the previous study, since the electron transfer in large π-conjugated systems has strong distance dependence, the V term can be calculated with [6],

(S8)

where V0 is the electron coupling without considering the distance dependence, β is the damped exponential, d is the separation distance from the dye LUMO/HOMO center to the TiO2 surface for the electron injection /recombination process. As seen in Figure S4, because the studied dyes’ HOMO is mainly localized in TPA, EDOT, and π-bridge units, while their LUMO is centered on the π-bridge and acceptor, we defined the centroid of TPA, EDOT, and π-bridge segments as the HOMO center. Similarly, the LUMO center was set to the centroid of the π-bridge and acceptor (Figure S5). According to the recent reports, the β was set to 0.5/1.0 for the electron injection/recombination process [7-8].

In this work, the V0 in Eq(S8) was calculated with the direct-coupling (DC) method [9-10], which can provide more accurate V0 value than the other methods, since it involves the orbital overlap correction. In terms of this method, the V0 can be estimated with [11],

(S9)

where Tij is the electron coupling without considering the orbital overlap correction, Sij is the spatial overlap integral, and ei/ej is the site energy. The Tij, Sij, and ei/ej can be calculated via Tij=<ψi|FKS|ψj>, Sij=<ψi|ψj>, and ei/ej=<ψi/ψj|FKS| ψi/ψj>. Among them, ψi is the HOMO/LUMO of dye, ψj is the LUMO of TiO2, and FKS is the Kohn-Sham matrix of dye/(TiO2)38 complex.

References

[1] J. Preat, C. Michaux, D. Jacquemin, and E.A. Perpete, J. Phys. Chem. C 113, 16821 (2009). doi:10.1021/jp904946a.

[2] M. Malagoli and J.L. Bredas, Chem. Phys. Lett. 327, 13 (2000). doi:10.1016/S0009-2614(00)00757-0.7.

[3] H.-Y. Chen and I. Chao, Chem. Phys. Lett. 401, 539 (2005).doi:10.1016/j.cplett.2004.11.125.

[4] H. Wei, J.-W. Luo, S.-S. Li, and L.-W. Wang, J. Am. Chem. Soc.138, 8165 (2016). doi:10.1021/jacs.6b03524.

[5] E. Maggio, N. Martsinovich, and A. Troisi, J. Chem. Phys. 137, 22A508 (2012). doi:10.1063/1.4737101.

[6] J.N. Clifford, E. Palomares, M.K. Nazeeruddin, M. Grätzel, J. Nelson, X. Li, N.J. Long, and J.R. Durrant, J. Am. Chem. Soc. 126, 5225 (2004). doi:10.1021/ja039924n.

[7] T.J. Barr and G.J. Meyer, ACS Energy Lett. 2, 2335 (2017). doi:10.1021/acsenergylett.7b00569.

[8] J.N. Clifford, E. Palomares, M.K. Nazeeruddin, M. Grätzel, J. Nelson, X. Li, N.J. Long, and J.R. Durrant, J. Am. Chem. Soc. 126, 5225 (2004). doi:10.1021/ja039924n.

[9] S. Yin, Y. Yi, Q. Li, G. Yu, Y. Liu and Z. Shuai, J. Phys. Chem. A 110, 7138 (2006). doi:10.1021/jp057291o.

[10] A. Troisi and G. Orlandi, J. Phys. Chem. A 110, 4065 (2006). doi:10.1021/jp055432g.

[11] S. Yin, L. Li, Y. Yang, and J.R. Reimers, J. Phys. Chem. C 116, 14826 (2012). doi:10.1021/jp303724r.

# Footnotes

( Corresponding author: Tel.: +86 916 2640660

E-mail address: zhaocb@snut.edu.cn (C. Zhao), yuxiaohu950203@163.com (X. Yu), jinlx@snut.edu.cn (L. Jin).

(