Supporting information：

The effect of EVA PWI on the viscosity/apparent viscosity of the model waxy oils is described in Figure S1. Obviously, adding the EVA PWI can improve the flowability of the oil samples at temperatures ≤ WAT, and the improving efficiency enhances with the increase of EVA concentration.

Figure S1.  Viscosity-temperature curves of model waxy oils.

Figure S2.  Schematic diagram of the in-house Couette rotating wax deposition device.

Figure S3.  Structure of the in-house Couette rotating wax deposition device.

(a)

(b)

Figure S4.  Macroscopic morphologies of the surface (a) and bottom (b) wax deposits formed by synthetic oil Ⅲ at 6h, and DSC properties (c) and wax precipitation characteristics (d) of the surface/bottom wax deposit.

(a)

(b)

Figure S5.  Macroscopic morphologies of the surface (a) and bottom (b) wax deposits formed by synthetic oil Ⅳ at 6h, and DSC properties (c) and wax precipitation characteristics (d) of the surface/bottom wax deposit.

(a)

(b)

Figure S6.  Macroscopic morphologies of the surface (a) and bottom (b) wax deposits formed by synthetic oil Ⅴ at 6h, and DSC properties (c) and wax precipitation characteristics (d) of the surface/bottom wax deposit.

# Text boxes

Sample barrel

Lifting mechanism

Hot bath

Conveyor

Torque sensor

Cold bath