Supplementary Materials

Doping effects of fluorinated chiral dopant in blue phase liquid crystals and its electro-optical behavior

Liang Gao 1, Hong-Mei Ma2 and Yu-Bao Sun 1,2,*

1	School of Electronic and Information Engineering, Hebei University of Technology, 5340 Xiping Road, Tianjin 300401, China;

2	Department of Applied Physics, Hebei University of Technology, 5340 Xiping Road, Tianjin 300401, China;

*	Correspondence: sun_yubao@163.com;

Supplementary Material 1: Determination of the helical twist power of the BD-F

From the experimental data, the distance between the disclinations R=507.50 μm when the concentration of the fluorinated chiral agent BD-F was 1.1 wt%. And for the Cano wedge cell, the wedge angle θ=0.01937 rad. So the pitch of CLC was obtained by P=2Rtanθ=2*507.5*0.01937=19.66 μm. On the other hand, the pitch of CLC was determined by the equation P=1/(HTP*Xc), where HTP were the helical twist power and Xc is the concentration of the doped chiral agent [1]. Therefore the HTPBD-F=1/(19.66*0.011)=4.6 μm-1.

Supplementary Material 2: Determination of the pitch of the BF sample and NBF sample

For the BF sample, the mixture including 94.3 wt% LC host (TEB300, Slichem), two kinds of chiral dopants 3.7 wt% R5011 (HTP=108 μm-1) and 2.0 wt% BD-F (HTP=4.6 μm-1, left- or right-handed chirality). So we can get the BF sample PBF=1/(PR5011XC-R5011+PBD-FXC-BD-F)=0.245 μm or PBF=1/(PR5011XC-R5011-PBD-FXC-BD-F)=0.256 μm [2,3]. Note that the total amount of chiral material increases to 5.7 wt% in the BF sample. Similarly, the pitch of the NBF sample was calculated by PNBF=1/(108*0.037)=0.250 μm. From Fig. 5, we know the reflection peak wavelength of BF sample is a little larger than that of NBF sample, so the pitch of BF sample is small larger than that of NBF sample, as a result, the chirality of BD-F is inverse to that of R5011.

References

[1] McConney ME, White TJ, Tondiglia VP, et al. Dynamic high contrast reflective coloration from responsive polymer/cholesteric liquid crystal architectures. Soft Matter 2012;8:318-323.

[2] Liu YJ, Wu PC, Lee W. Spectral variations in selective reflection in cholesteric liquid crystals containing opposite-handed chiral dopants. Mol. Cryst. Liq. Cryst. 2014;596:37-44.

[3] Sun PZ, Liu Z, Wang W, et al. Light-reconfigured waveband-selective diffraction device enabled by micro-patterning of a photoresponsive self-organized helical superstructure. J. Mater. Chem. C 2016;4:9325-9330.