Supplementary  Information

Table S1 Summery of the optical, photoelectronic and DFT calculation results

| Compound | IP(eV) | λmax(nm)a） | Egopt(eV) | EHOMO (eV) |  |  | ELUMO (eV) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Exp.b) | Calcd.d) |  | Exp.c) | Calcd.d) |
| Dibenzo-CDI 1 | 6.22 | 606 | 2.04 | -6.22 | -2.98 |  | -4.18 | -2.98 |
| Dibenzo-CDI 2 | 6.24 | 606 | 2.04 | -6.24 | -2.98 |  | -4.20 | -2.98 |
| Dibenzo-CDI 3 | 6.21 | 581 | 2.13 | -6.21 | -6.21 |  | -4.08 | -2.92 |
| a)The optical bandgap was calculated according to Egopt= 1240/λmax; b) EHOMO = -IP; c) Estimated from the empirical equation ELUMO = IP - Egopt ; d) Determined from DFT calculation at the B3LYP/6-31G(d) level using the Gaussian 09 program package. |  |  |  |  |  |  |  |  |

Figure S1 DSC curves of Dibenzo-CDI 1, 2, 3 (Note: These figures are from our previously reported work “J. Org. Chem. 78 (2013) 4857”.)

Figure S2 Optical micrograph of Dibenzo-CDI 3 at 190℃

Figure S3 XRD diffraction patterns of (a) Dibenzo-CDI 2 at 120℃ and (b) Dibenzo-CDI 3 at 190℃. The insets are the schematic diagrams of molecular stackings.

a)

b)

Figure S4 Photocurrents of Dibenzo-CDI 1 at (a) 170 ℃, (b) 80 ℃.

Figure S5 Photocurrents of Dibenzo-CDI 2 at 150 ℃.

Figure S6 Photocurrents of Dibenzo-CDI 3 at 30 ℃ and 160 ℃,respectively.