SYNTHESIS AND CHARACTERIZATION OF SILICA SUPPORTED SCHIFF BASE LIGANDS AND THEIR METAL COMPLEXES: APPLICATIONS AS CATALYSTS FOR THE OXIDATION OF ALKANES

Esin Ispir

Faculty of Science and Arts, Chemistry Department, K.Maraş Sütçü Imam University, Kahramanmaraş, 46100, Turkey

E-mail: esinispir@ksu.edu.tr

Supplemental Materials

- (b)

(c)

Figure S 1: SEM images of silica gel (a), APS (b) and L1H (c)

Table S 1: Thermogravimetric Data of Ligand and Complexes

| Compound | TG Range/oC | Mass loss/% Teorical (Calculated) | Assignment |
| --- | --- | --- | --- |
| L1H | 20-150 | (5.74) | Loss of water |
|  | 150-900 | 14.15 (13.20) | Ligand decomposition |
|  | 900- | 85.85 (81.06) | SiO2 |
| L2H | 20-150 | (3.25) | Loss of water |
|  | 150-900 | 16.11 (15.20) | Ligand decomposition |
|  | 900- | 83.89 (81.55) | SiO2 |
| L3H | 20-150 | (1.72) | Loss of water |
|  | 150-900 | 15.14 (14.50) | Ligand decomposition |
|  | 900- | 84.86 (83.79) | SiO2 |
| Cu(L1)(AcO).H2O | 20-900 | (2.71) | Loss of water |
|  |  | 16.70 (15.52) | Complex decomposition |
|  | 900- | 83.30 (81.77) | SiO2 +CuO |
| Co(L1)(AcO).H2O | 20-900 | (1.68) | Loss of water |
|  |  | 15.28 (14.93) | Complex decomposition |
|  | 900- | 84.72 (83.39) | SiO2 +Co3O4 |
| Cu(L2)(AcO).H2O | 20-900 | (2.03) | Loss of water |
|  |  | 16.35 (15.80) | Complex decomposition |
|  | 900- | 83.65 (82.17) | SiO2 +CuO |
| Co(L2)(AcO).H2O | 20-900 | (2.77) | Loss of water |
|  |  | 14.80 (14.13) | Complex decomposition |
|  | 900- | 85.20 (83.10) | SiO2 +Co3O4 |
| Cu(L3)(AcO).H2O | 20-900 | (1.62) | Loss of water |
|  |  | 15.05 (14.19) | Complex decomposition |
|  | 900- | 84.95 (84.55) | SiO2 +CuO |
| Co(L3)(AcO).H2O | 20-900 | (1.20) | Loss of water |
|  |  | 14.00 (12.83) | Complex decomposition |
|  | 900- | 86.00 (85.97) | SiO2 +Co3O4 |

Figure S 2: TG-DTA of the silica supported ligand (L1H)

Figure S 3: TG-DTA of Cu(L1)(AcO).H2O