Supplemental material

Electric field assisted-unidirectional hybrid films of carbon nanotubes and liquid crystal polymer for light modulation

Weiwei Tiea,b, Surjya Sarathi Bhattacharyyad, Zhi Zhenga,b, Kyung Jun Choc, Tae Hyung Kimc, Young Jin Limc, and Seung Hee Leec*

a Key Laboratory of Micro-Nano Materials for Energy Storage and Conversion of Henan Province, School of Advanced Materials and Energy, Institute of Surface Micro and Nanomaterials, Xuchang University, Xuchang, Henan, 461000, China

b Henan Joint International Research Laboratory of Nanomaterials for Energy and Catalysis, Xuchang University, Xuchang, Henan 461000, China

c Applied Materials Institute for BIN Convergence, Department of BIN Convergence Technology and Graduate School of Flexible & Printable Electronics Engineering, Chonbuk National University, Jeonju, Jeonbuk 54896, South Korea

d Asutosh College, 92, Shyamaprasad Mukherjee Road, Kolkata, 700 026, West Bengal, India

Figure S1. Scanning electron microscopic images of m-CNTs

The length of m-CNTs are has been investigated by Scanning electron microscopy shown in Figure S1. It is observed that the f-CNTs normally possess lengths of approximately 100-500 nm, which indicates f-CNTs are further shortened by acid oxidation cutting. This variety maybe beneficial to their subsequent dispersion and field induced alignment process.