Aryl ethers decorated gallic acid-naphthalimide conjugate: Aggregation and sensing toward amines and F-

Chiranjit Pati, Kumaresh Ghosh*

Department of Chemistry, University of Kalyani, Kalyani-741235, India. Email:ghosh_k2003@yahoo.co.in, kumareshchem18@klyuniv.ac.in Fax: +913325828282; Tel: +913325828750 Extn: 305.

.

Table 1S.  Results of gelation test for compound 1.

| Solvents | Results |
| --- | --- |
| THF | S |
| 1,2-dichlorobenzene- dioxane (5:1, v/v) | G (6 ) |
| 1,2- dichloroethane | PG |
| DMSO | G (20) |
| Toluene- dioxane (5:1, v/v) | G (6) |
| CH3CN- dioxane (5:1, v/v) | G (8) |
| dioxane | S |
| CHCl3 | PS |
| CCl4 | PS |
| MeOH | I |
| S = Solution; G = Gel (minimum gelation concentration; mg/ ml); PG = partial gel; I = Insoluble; PS = partial soluble |

(C)

Fig. 1S.  (A) Partial FTIR spectra of 1 in (a) amorphous state, (b) gel state obtained from CH3CN-1,4-dioxane (5:1, v/v); (B) Pictorial  presentation of thermo-reversibilly of the gel states obtained from CH3CN-1,4-dioxane (5:1, v/v) and Toluene-1,4-dioxane (5:1, v/v); (C) Plot of Tgel with varying concentration of gelator 1 in different solvents.

Fig. 2S.  (a) Partial 1H NMR (400 MHz, d6- DMSO) of 1 at different concentrations at 25oC (i) 0.02 M, (ii) 0.017 M, (iii) 0.014 M, (iv) 0.012 M, (v) 0.011 M, (vi) 0.01 M, (vii) 0.009 M; (b) Change in chemical shift ((( in ppm) of the indicated protons with concentration of 1.

(a)

Fig. 3S. (a) Pictorial representation of the sensitivity of the gel of 1 in toluene-1,4-dioxane (5:1, v/v) in presence of 1 equiv. amount of  n-butylamine (c = 0.1 M); (b) Partial 1H NMR (d6- DMSO, 400 MHz) of (i) 1 (c = 5.53 x 10-3 M) and (ii) 1 in the presence of 1 equiv. amount of n-butylamine followed treatment with (iii) acetic acid.

(a)                                                          (b)                                                                         (b)

Fig. 4S. (a) Comparison of emission spectra of CH3CN-1,4-dioxane (5:1, v/v) gel of 1 in the absence and presence of n-butylamine (λex = 445 nm); (b) Partial 1H NMR spectra (400 MHz, d6- DMSO) of (i) 1 (c = 5.87 x 10-3 M) and (ii) 1 in the presence of 5 equiv. amounts of aniline.

Fig. 5S. (A) Partial FTIR spectra of gel of 1 (prepared from CH3CN-1,4-dioxane (5:1, v/v)) (a) in absence and (b) presence of n-butylamine; (B) SEM image of the n-butylamine treated xerogel.

Fig. 6S. Pictorial representation of thermo-reversibility of 1 equivalent amount of n-butylamine (c = 0.1 M) treated gel of 1 in CH3CN-1,4-dioxane (5:1, v/v).

Fig. 7S. (a) Amplitude and (b) Frequency sweep experiments of CH3CN-1,4-dioxane (5:1, v/v) gel of 1 without and with 1 equiv. amount of n-butylamine (c = 0.1 M). Amplitude sweep experiment was carried out at constant frequency of 1Hz and frequency sweep experiment was conducted at constant 0.1 % strain. Gelator concentration was 8 mg/mL.

Table 2S. Summary of the rheological properties of the gels of 1 in CH3CN-1,4-dioxane (5:1,

v/v)

* G′av and G′′av values were calculated from frequency sweep data.

Fig. 8S. Vapor phase detection through color change: (a) in presence of 1 equiv. amount of n-butylamine (c = 0.1 M) and (b) NH3 using CH3CN-1,4-dioxane (5:1, v/v) gel of 1.

Fig. 9S. UV-vis titration spectra of 1 (c = 2.50 x 10-5 M) upon addition of (a) ethanolamine, (b) N2H4, (c) NH2OH, (d) aniline, (e) pyridine, (f) dimethylamine (DMA), (g) Et3N (c = 1.0 x 10-2 M) in CH3CN containing 1% THF.

Fig. 10S. Change in absorbance of 1 (c = 1 x 10-4 M) upon addition of 40 equiv. amounts of n-butylamine (c = 1.0 x 10-2 M) in CH3CN containing 1% THF; (b) Color change of 1 (c = 1 x 10-4 M) upon addition of 40 equiv. amounts of n-butylamine (c = 1.0 x 10-2 M) in CH3CN containing 1% THF.

Fig. 11S. (a) Benesi–Hilderband plots for 1 (c = 2.5 x 10-5 M) with (a) n-butylamine, (b) dimethylamine (DMA), (c) triethylamine (Et3N) (c = 1.0 x 10-3 M) at 442 nm from UV-vis study in CH3CN containing 1% THF.

Fig. 12S. (a) Change in absorbance of 1 (c = 2.50 x 10-5 M) with n-butylamine followed by addition of acetic acid (c = 1.0 x 10-2 M) in CH3CN containing 1% THF; (b) Color change upon addition of n-butylamine followed by acetic acid.

Fig. 13S. Change in emission of 1 (c = 2.50 x 10-5 M) upon addition of (a) n-butylamine, (b) dimethylamine, (c) Et3N, (d) ethanolamine, (e) N2H4, (f) NH2OH, (g) aniline, (h) pyridine (c = 1.0 x 10-2 M) containing 1% THF in CH3CN ( λex = 445 nm).

Fig. 14S. Comparison of normalized UV-vis spectra of toluene-1,4-dioxane (5:1, v/v) gel of 1 before and after treatment with F- ions; (b) Partial FTIR spectra of gel of (i) 1 [prepared from toluene-1,4-dioxane (5:1, v/v)] and (ii) gel of 1 with F- ions.

Fig. 15S. SEM image of the xerogel of 1 prepared from toluene-1,4-dioxane (5:1, v/v) after treatment with F- ions.

Fig. 16S. Photograph showing the changes in gel state of 1 in CH3CN-1,4-dioxane (5:1 v/v) (c = 6 mg/mL) upon addition of 1 equiv. amount of different anions (c = 0.08 M) after 25 min.

Fig. 17S. Change in absorbance of 1 (c = 2.5 x 10-5 M) from 0 up to 15 equiv. amounts of tetrabutylammonium salts of (a) F-, (b) AcO-, (c) DHP, (d) Cl-, (e) Br-, (f) I-, (g) HSO4- (c =1 x 10-3 M) in 1% THF in CH3CN.

Fig. 18S. Change in absorbance of 1 (c =2.5 x 10-5 M) upon addition of 15 equiv. amounts of F-, AcO- and H2PO4- (DHP) (c =1 x 10-3 M) ions as their tetrabutylammonium salts followed by addition of 4 equiv. amounts of (a) Fe(ClO4)3, (b) BF3 and Ca(ClO4)2 (c =1 x 10-3 M) in CH3CN containing 1% THF; (d) Change in color of the solution of 1 (c =2.5 x 10-5 M) in CH3CN containing 1% THF during the experiments mentioned in (a), (b) and (c).

Fig. 19S. Change in (a) color and (b) absorbance of 1 (c =2.5 x 10-5 M) upon addition of 15 equiv. amounts of each anions (c =1 x 10-3 M) followed by addition of 6 equiv. amounts of AgClO4 (c =1 x 10-3 M) in CH3CN containing 1% THF.

Fig. 20S. Change in (a) absorbance and (b) color of 1 (c = 2.5 x 10-5 M) in CH3CN containing 1% THF upon addition of 15 equiv. amounts of tetrabutylammonium hydroxide (c =1 x 10-3 M).

Fig. 21S. Change in absorbance of 1 (c = 2.5 x 10-5 M) in presence of 15 equiv. amounts of (a) F-, (b) AcO- and then upon gradual addition of H2O.

Fig. 22S. Change in colour of 1 (c = 2.5 x 10-5 M) in presence of 15 equiv. amounts of F- and AcO- followed by addition of H2O.

Fig. 23S. (a) Absorbance ratio of  1 (c = 2.5 x 10-5 M)  at 620 nm upon addition of 15 equiv. amounts of  F-  ions to the solution containing 15 equiv. amounts other anions in CH3CN containing 1% THF and (b) the associated color changes.

Fig. 24S. Change in emission (λex = 445 nm) of 1 (c = 2.5 x 10-5 M) upon addition of 8 equiv. amounts of tetrabutylammonium salts of (a) AcO-, (b) DHP, (c) Cl-, (d) Br-, (e) I-, (f) HSO4-, (g)  OH-  (c = 1 x 10-3 M) in  CH3CN containing 1% THF.

Fig. 25S. (a) UV-vis Job plot of 1 with F- at 445 nm in CH3CN containing 1% THF where [H] = [G] = 2.5 x 10-5 M; (b) Non linear fitting of the titration data for 1 (c = 2.5 x 10-5 M) with F- (c = 1.0 x 10-3 M) at 508 nm in CH3CN containing 1% THF and (c) Detection limit of 1 (c = 2.5 x 10-5 M) for F- (c = 1.0 x 10-3 M) in CH3CN containing 1% THF.

Fig. 26S. The color change of gel phase of 1 in toluene-1,4-dioxane (5:1 v/v)  (c = 6 mg/mL) upon addition of different equiv. amounts of  TBAF (c = 0.08 M).

Fig. 27S. 1H NMR (400 MHz) of compound 5 in CDCl3 containing few drops of d6-DMSO.

Fig. 28S. 13C NMR of 5 in CDCl3 containing two drops of d6-DMSO (100 MHz).

Fig. 29S. HRMS spectrum of 5.

Fig. 30S. 1H NMR (400 MHz) of compound 1 in d6-DMSO.

Fig. 31S. 13C NMR (100 MHz) of 1 in d6-DMSO.

Fig. 32S. HRMS spectrum and isotopic mass distribution of compound 1.

# Text boxes

| Gels | Crossover (% strain) | G′av (Pa)* | G′′av (Pa)* |
| --- | --- | --- | --- |
| 1 | 3.5 | 52400 | 8150 |
| 1 with n-butylamine | 1.3 | 8530 | 1081 |