Oxidative removal of sulfadiazine using synthetic and natural manganese dioxides

Ardie Septian, Sanghwa Oh, and Won Sik Shin*

School of Architecture, Civil, Environmental and Energy Engineering, Kyungpook National University, Daegu 41566, Korea

# *Corresponding author: Professor, Phone: +82-53-950-7584; Fax: +82-53-950-6579; E-mail: wshin@mail.knu.ac.kr

# Supporting Information

Table S1. Effect of temperature on the rate constant (kT) of SDZ oxidation. Number in the parenthesis indicates standard deviation in 95% confidence interval.

| pH | MnO2 | Temperature ((C) |  | R2 | SSE | p-value |
| --- | --- | --- | --- | --- | --- | --- |
| 5 | Birnessite | 10 | 0.493 (( 0.014) | 0.998 | 3.800 ( 10(5 | 5.000 ( 10(5 |
|  |  | 20 | 0.522 (( 0.016) | 0.997 | 5.400 ( 10(5 | 7.000 ( 10(5 |
|  |  | 30 | 0.885 (( 0.014) | 0.999 | 4.300 ( 10(5 | 1.000 ( 10(5 |
|  |  | 40 | 0.938 (( 0.013) | 0.999 | 3.300 ( 10(5 | 1.000 ( 10(5 |
| 5 | Natural MnO2 | 10 | 0.282 (( 0.009) | 0.998 | 1.500 ( 10(5 | 6.000 ( 10(5 |
|  |  | 20 | 0.520 (( 0.014) | 0.998 | 4.200 ( 10(5 | 5.000 ( 10(5 |
|  |  | 30 | 0.550 (( 0.013) | 0.998 | 3.600 ( 10(5 | 3.000 ( 10(5 |
|  |  | 40 | 0.548 (( 0.009) | 0.999 | 1.600 ( 10(5 | 1.000 ( 10(5 |
| 8 | Birnessite | 10 | 0.334 (( 0.068) | 0.993 | 9.400 ( 10(4 | 0.016 |
|  |  | 20 | 0.479 (( 0.017) | 0.996 | 6.100 ( 10(5 | 1.000 ( 10(4 |
|  |  | 30 | 0.861 (( 0.004) | 0.999 | 2.600 ( 10(6 | 0.000 |
|  |  | 40 | 0.867 (( 0.013) | 0.999 | 3.600 ( 10(5 | 1.000 ( 10(5 |
| 8 | Natural MnO2 | 10 | 0.232 (( 0.041) | 0.975 | 3.400 ( 10(4 | 0.011 |
|  |  | 20 | 0.532 (( 0.012) | 0.999 | 2.700 ( 10(5 | 2.000 ( 10(5 |
|  |  | 30 | 0.548 (( 0.006) | 0.999 | 7.900 ( 10(6 | 0.000 |
|  |  | 40 | 0.530 (( 0.010) | 0.999 | 1.900 ( 10(5 | 1.000 ( 10(5 |

Unit: temperature = ((C);  = (mmol L(1 hr(1). Calculated at C0 of MnO2 = 11.49 mmol L(1 and C0 of SDZ = 0.4 mmol L(1.

Table S2. Thermodynamic parameters of SDZ oxidation.

| pH | MnO2 | Temperature (K) | Ea | Δ‡H | Δ‡S | Δ‡G |
| --- | --- | --- | --- | --- | --- | --- |
| 5 | Birnessite | 283 | 0.005 | (1.422 | 0.004 | (2.628 |
|  |  | 293 |  | (1.472 |  | (2.721 |
|  |  | 303 |  | (1.522 |  | (2.813 |
|  |  | 313 |  | (1.572 |  | (2.906 |
| 5 | Natural | 283 | 0.004 | (1.212 | 0.003 | (2.209 |
|  | MnO2 | 293 |  | (1.255 |  | (2.287 |
|  |  | 303 |  | (1.298 |  | (2.365 |
|  |  | 313 |  | (1.341 |  | (2.443 |
| 8 | Birnessite | 283 | 0.007 | (2.007 | 0.006 | (3.799 |
|  |  | 293 |  | (2.078 |  | (3.933 |
|  |  | 303 |  | (2.149 |  | (4.068 |
|  |  | 313 |  | (2.220 |  | (4.202 |
| 8 | Natural | 283 | 0.005 | (1.477 | 0.004 | (2.740 |
|  | MnO2 | 293 |  | (1.530 |  | (2.837 |
|  |  | 303 |  | (1.582 |  | (2.933 |
|  |  | 313 |  | (1.634 |  | (3.030 |

Units: temperature = (K); ΔH = (kJ mol(1); ΔS = (kJ K(1 mol(1); ΔG = (kJ mol(1); Ea = (kJ mol(1). R = 8.314 ( 10(3 kJ mol(1. Calculated at C0 of MnO2 = 11.49 mmol L(1 and C0 of SDZ = 0.4 mmol L(1.