Supporting Information

Synthesis and Characterization of Fluorene Derivatives as Organic Semiconductors for Organic Field-Effect Transistor.

Kwanghee Cho,a† M. Rajeshkumar Reddy,b † Dongkyu Kim,a Dongil Ho,a Chaeyoung Yun,b SungYong Seo,b* and Choongik Kima*

a Department of Chemical and Biomolecular Engineering, 35 Baekbeom-ro, Mapo-gu, Sogang University, Seoul 04107, Korea

b Department of Chemistry, Pukyong National University, Busan 48513, Korea

* Corresponding authors

E-mail addresses: choongik@sogang.ac.kr (C. Kim), syseo@pknu.ac.kr (S. Seo)

† These authors contributed equally to this work.

Keywords: fluorene; organic field effect transistors; organic semiconductor; solution process

Table S1. OTFT Device performance on the Various fabrication conditions of compound 4 including solvent, concentration, substrate, and substrate temperature. (µ: Carrier mobility, Ion/Ioff : Current on/off ratio, VT: Threshold voltage).a

| Solvent | Concentration (mg/mL) | Substrate Temperature (℃) b | Substrate | µhmax µhavg (cm2/Vs) | VTavg(V) | Ion/Ioff |
| --- | --- | --- | --- | --- | --- | --- |
| Chloroform | 1 | 37 (60 %) | SiO2 | - |  |  |
|  |  |  | PTS |  |  |  |
|  |  |  | PS-brush |  |  |  |
|  |  | 42 (70 %) | SiO2 | - |  |  |
|  |  |  | PTS |  |  |  |
|  |  |  | PS-brush |  |  |  |
|  |  | 50 (80 %) | SiO2 | - |  |  |
|  |  |  | PTS |  |  |  |
|  |  |  | PS-brush |  |  |  |
|  | 4 | 37 (60 %) | SiO2 | - |  |  |
|  |  |  | PTS |  |  |  |
|  |  |  | PS-brush |  |  |  |
|  |  | 42 (70 %) | SiO2 | - |  |  |
|  |  |  | PTS |  |  |  |
|  |  |  | PS-brush |  |  |  |
|  |  | 50 (80 %) | SiO2 | - |  |  |
|  |  |  | PTS |  |  |  |
|  |  |  | PS-brush |  |  |  |
| Toluene | 1 | 70 (60 %) | SiO2 | - |  |  |
|  |  |  | PTS |  |  |  |
|  |  |  | PS-brush |  |  |  |
|  |  | 80 (70 %) | SiO2 | - |  |  |
|  |  |  | PTS |  |  |  |
|  |  |  | PS-brush |  |  |  |
|  |  | 90 (80 %) | SiO2 | - |  |  |
|  |  |  | PTS |  |  |  |
|  |  |  | PS-brush |  |  |  |
|  | 4 | 70 (60 %) | SiO2 | 0.0005 (0.00039 ± 0.000097) | 54.1 ± 4.46 | (9.0 ± 5.2) ×103 |
|  |  |  | PTS | 0.0055 (0.0022 ± 0.0021) | 37.2 ± 3.47 | (9.1 ± 3.6) ×104 |
|  |  |  | PS-brush | 0.0006 (0.00047 ± 0.000078) | 47.5 ± 8.35 | (3.7 ± 1.1) ×104 |
|  |  | 80 (70 %) | SiO2 | - |  |  |
|  |  |  | PTS |  |  |  |
|  |  |  | PS-brush |  |  |  |
|  |  | 90 (80 %) | SiO2 | - |  |  |
|  |  |  | PTS |  |  |  |
|  |  |  | PS-brush |  |  |  |

a All devices were measured in vacuum and the device characteristics were calculated using 6 different measurements. b ratio to boiling point in chloroform and toluene.

Figure S1 AFM topographic images of drop-casted films of compound 1 (A), 2 (B), and 3 (C). Scale bars indicate 5 µm.

Figure S2. Reliability for OTFT Device performance fabricated on SiO2(A), PTS(B), and PS-brush(C) of compound 4.