Structural properties and thermal behavior of novel interaction product 4-amino-5-(furan-2-yl)-4H-1,2,4-triazole-3-thione with molecular iodine

Victoria A. Ivolginaa, Margarita S. Chernov’yantsa, Leonid D. Popova, Vitaliy V. Suslonovb, Natalya A. Avtushenkoa, Nikolay V. Luanguzova

aDepartment of Chemistry, Southern Federal University, Zorge St. 7, 344090 Rostov-on-Don, Russia

bSt.Petersburg State University, 7/9 Universitetskaya nab., St. Petersburg, 199034 Russia

Email: vickaivolgina@yandex.ru

Supplemental Materials

Table S 1: Crystal data and structure refinement for C6H6N4OS∙I2

| Compound | 1 |
| --- | --- |
| Empirical Formula | C6H6I2N4OS |
| Formula Weight | 436.01 |
| Crystal System / Space Group | Monoclinic/ P21 |
| a / Å | 10.4679(6) |
| b / Å | 4.6885(3) |
| c / Å | 11.6913(8) |
| / ° | 90 |
| β / ° | 92.903(6) |
| γ / ° | 90 |
| V / Å3 | 573.06(7) |
| Z | 2 |
| D calc (g/cm3) | 2.527 |
| μ (mm-1) | 44.641 |
| Crystal size (mm) | 0.1 × 0.05 × 0.05 |
| Color / Shape | Dark-brown/ needle-like |
| Temp (K) | 100(2) |
| Theta range for collection | 7.572 to 144.99 |
| Reflections collected | 4909 |
| Independent reflections | 2259 [Rint = 0.0628, Rsigma = 0.0762] |
| Data/restraints/parameters | 2259/1/128 |
| Goodness of fit on F2 | 1.048 |
| Final R indices [I > 2σ(I)] | R1 = 0.0423, wR2 = 0.0989 |
| R indices (all data) | R1 = 0.0458, wR2 = 0.1020 |
| Largest difference peak/hole | 1.13/-0.99 |

| Table S 2: Bond Lengths for C6H6N4OS∙I2 |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Atom | Atom | Length/Å |  | Atom | Atom | Length/Å |
| I1 | I2 | 2.82(11) |  | N4 | C5 | 1.30(16) |
| I1 | S1 | 2.80(3) |  | C5 | C2 | 1.45(2) |
| S1 | C10 | 1.69(14) |  | O6 | C7 | 1.37(17) |
| N1 | N3 | 1.40(13) |  | O6 | C2 | 1.37(16) |
| N1 | C10 | 1.37(18) |  | C7 | C8 | 1.36(2) |
| N1 | C5 | 1.36(18) |  | C8 | C1 | 1.42(2) |
| C10 | N2 | 1.33(17) |  | C1 | C2 | 1.35(19) |
| N2 | N4 | 1.37(16) |  |  |  |  |

| Table S 3: Bond Angles for C6H6N4OS∙I2 |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Atom | Atom | Atom | Angle/˚ |  | Atom | Atom | Atom | Angle/˚ |
| S1 | I1 | I2 | 171.74(8) |  | N1 | C5 | C2 | 125.3(11) |
| C10 | S1 | I1 | 97.4(5) |  | N4 | C5 | N1 | 111.1(12) |
| C10 | N1 | N3 | 126.9(11) |  | N4 | C5 | C2 | 123.5(12) |
| C5 | N1 | N3 | 124.8(12) |  | C7 | O6 | C2 | 106.5(11) |
| C5 | N1 | C10 | 108.1(10) |  | C8 | C7 | O6 | 110.3(12) |
| N1 | C10 | S1 | 126.6(10) |  | C7 | C8 | C1 | 106.2(12) |
| N2 | C10 | S1 | 130.1(11) |  | C2 | C1 | C8 | 106.9(13) |
| N2 | C10 | N1 | 103.2(11) |  | O6 | C2 | C5 | 113.9(11) |
| C10 | N2 | N4 | 113.8(10) |  | C1 | C2 | C5 | 136.0(13) |
| C5 | N4 | N2 | 103.6(11) |  | C1 | C2 | O6 | 110.1(13) |

Table S 4: Bond lengths and torsion angles (Å, °)

Bond lengths (Å) I(1)-I(2) - 2.8182(11) I(1)-S(1) - 2.798(3) S(1)-C(10) - 1.687(14)

Torsion angles (°) I(2)-I(1)-S(1)-C(10): -102.3(7) I(1)-S(1)-C(10)-N(1): 134(1) I(1)-S(1)-C(10)-N(2): -45(1)

Bond angles (°) I(2)-I(1)-S(1): 2.0583(6) I(1)-S(1)-C(10): 171.74(8)

Figure S 1: Mass-spectra of C6H6N4OS∙I2

Figure S 2: Raman spectrum of C6H6N4OS∙I2

Figure S 3: FT-IR spectrum of C6H6N4OS∙I2

Figure S 4: 1H NMR (250 MHz, DMSO) of C6H6N4OS∙I2

Figure S 5: 13C NMR (62.9 MHz, DMSO) of C6H6N4OS∙I2

Figure S 6:  1H NMR (600 MHz, DMSO) of 4-amino-5-(furan-2-yl)-4H-1,2,4-triazole-3-thione

Figure S 7:  13C (151 MHz, DMSO) of 4-amino-5-(furan-2-yl)-4H-1,2,4-triazole-3-thione