Supporting Information for:

# Discotic mesogens based on triphenylene-fused benzimidazole or perimidine: facile synthesis, mesomorphism, optical properties and self-assembly

Sheng-Yuan Fan, a Hong-Tian Xu,a Qiang-Gen Li,a Dong-Mei Fang, b Wen-Hao Yu,a Shi-Kai Xiang,a Ping Hu,a Ke-Qing Zhao, a Chun Feng *a and Bi-Qin Wang*a

a College of Chemistry and Materials Science, Sichuan Normal University, Chengdu, 610066, P.R. China.

b Chengdu Institute of Biology, Chinese Academy of Sciences, Chengdu 610041, P.R. China.

*E-mail: fengc@sicnu.edu.cn (feng_chun@126.com); wangbiqin1964@126.com

Contents:

TGA curves................................................................................................................ S2

DSC curves................................................................................................................. S3

POM images...............................................................................................................S6

Representative X-ray Diffractograms............................................................................S8

DFT Calculations………………………………………………......……………….…S11

UV-Vis and Fluorescence Data .................................................................................…S12

NMR.............…………………………..........................................................................S13

HRMS..................................... ....................................................................................…S16

- TGA

Figure S1. TGA curves of TPC6 anhydride, TPC8 anhydride, TDBI, TDNI, TDPI, and TDP. The measurements were performed under a nitrogen atmosphere, with heating and cooling rates of 10 oC min-1.

- Differential scanning calorimetry (DSC) curves

Figure S2. DSC curves of TPC6 anhydride, TPC8 anhydride, TDBI, TDNI, TDPI, and TDP. The measurements were performed under a nitrogen atmosphere, with heating and cooling rates of 10 oC min-1

- Polarizing optical microscopy images

TPC6 anhydride                            TPC8 anhydride

TDBI                                    TDNI

TDPI                                     TDP

Figure S3. Polarized optical microscopy (POM) images of the drop-casted thin film of TPC6 anhydride, TPC8 anhydride, TDBI, TDNI, TDPI, and TDP between two glass slides observed under two crossed polarizers upon slow cooling (1-2 oC min-1) from the isotropic phase: TPC6 anhydride at 253 oC; TPC8 anhydride at 230 oC; TDBI at 281 oC; TDNI at 245 oC; TDPI at 270 oC; TDP at 259 oC.

- X-ray diffraction (XRD)

Figure S4. Representative XRD data for TPC6 anhydride, TDBI, TDNI, TDPI, and TDP.

- DFT Calculations

Figure S5. Frontier molecular orbital profiles of TPC8 anhydride, TDBI, TDNI, TDPI and TDP based on DFT (B3LYP/6-31+G*) calculations (four alkoxy chains are replaced with methoxy groups for simplifying the calculations).

7. UV-Vis and Fluorescence Data

Figure S6. UV-Vis absorbance spectra of TPC8 anhydride, TDBI, TDNI, TDPI, and TDP in THF (10-5 M).

Figure S7. The normalized photoluminescence spectra of TPC8 anhydride, TDBI, TDNI, TDPI and TDP in THF solutions (10-5 M, red) and films (black).

7. NMR

Figure S8. NMR of TPC6 acid, TPC6 anhydride, TPC8 anhydride, TDBI, and TDP.

8. HRMS