Supporting Information

## Synthesis of novel ultraviolet stabilizers based on [60]fullerene and their effects on photo-oxidative degradation of polystyrene

Lipengcheng Xiaoa, Yang Zhaoa, Bo Jin*a, Qingchun Zhanga, Zuohu Chaia, Rufang Peng* a

aState Key Laboratory of Environmental Friendly Energy Materials, Southwest University of Science and Technology, Mianyang 621010, Sichuan, P. R. China.

E-mail: jinbo0428@163.com; pengrufang@swust.edu.cn;

Tel: +86-0816-2419011

Table of Contents

General Procedure for the Synthesis of [60]fullereropyrroline 2a-b	S1-3

1H NMR spectra and 13C NMR spectra of compounds 2a-b	S3-8

HRMS of compounds 2a-b	S8-9

HPLC of compounds 2a-b	S9-10

Water contact angle measurement of films	S10-11

General Procedure for the Synthesis of [60]fullereropyrroline 2a-b.

C60 (36.0 mg, 0.05 mmol), N-Benzylglycine (49.5 mg, 0.30 mmol), p-anisaldehyde (1a) (27.2 mg, 0.20 mmol) or 4-ethoxybenzaldehyde (1b) (30.0 mg, 0.20 mmol) and chlorobenzene (10 mL) were added into a 100 mL thick-walled glass bottle with a magnetic stirring bar. The reaction was stirred at 130 °C for 5 h with reflux. After the reaction was completed, the reaction solution was evaporated under vacuum, and the residue was chromatographed on a silica gel column eluting with CS2. The first purple band was unreacted C60, and the second brown band was eluted with toluene/hexane (1:1 v/v) to afford the desired product 2a-b.

Synthesis of 2a. The product was purified by silica gel chromatography (toluene: hexane = 1:1) to afford 2a (15.7 mg, 33%) as a brown amorphous solid and unreacted C60 (13.7 mg, 38%). 1H NMR (600 MHz, CDCl3/CS2 (3:1 v/v)) δ 7.60 (d, J = 7.4 Hz, 4H), 7.41 (t, J = 7.6 Hz, 2H), 7.31 (t, J = 7.4 Hz, 1H), 6.91 (d, J = 8.2 Hz, 2H), 5.12 (s, 1H), 4.81 (d, J = 9.4 Hz, 1H), 4.52 (d, J = 13.3 Hz, 1H), 4.10 (d, J = 9.4 Hz, 1H), 3.77 (s, 3H), 3.59 (d, J = 13.3 Hz, 1H). 13C NMR (150 MHz, CDCl3/CS2 (3:1 v/v)) δ 159.49, 156.11, 153.75, 153.28, 153.25, 147.05, 147.04, 146.56, 146.20, 146.12, 146.08, 146.04, 145.97, 145.94, 145.90, 145.86, 145.70, 145.70, 145.54, 145.34, 145.30, 145.26, 145.21, 145.18, 145.06, 145.02, 145.00, 144.90, 144.48, 144.44, 144.17, 144.14, 142.93, 142.77, 142.46, 142.39, 142.35, 142.33, 142.12, 142.03, 141.93, 141.90, 141.88, 141.80, 141.78, 141.73, 141.62, 141.43, 141.35, 139.97, 139.96, 139.77, 139.38, 137.61, 136.61, 136.31, 135.67, 135.54, 130.26, 128.59, 128.57, 128.50, 127.40, 114.03, 80.83(sp3-C of C60), 76.58(sp3-C of C60), 68.30, 66.43, 56.61, 54.74. UV−vis (toluene) λ/(nm): 287, 332, 433. HRMS (MALDI-TOF) m/z calcd for C76H17NO [M + H]+ 959.1305, found 959.1309.

Synthesis of 2b. The product was purified by silica gel chromatography (toluene: hexane = 1:1) to afford 2b (19.3 mg, 39%) as a brown amorphous solid and unreacted C60 (11.9 mg, 33%). 1H NMR (600 MHz, CDCl3/CS2 (3:1 v/v)) δ 7.61 (d, J = 7.3 Hz, 4H), 7.42 (t, J = 7.6 Hz, 2H), 7.32 (t, J = 7.4 Hz, 1H), 6.90 (d, J = 8.3 Hz, 2H), 5.12 (s, 1H), 4.82 (d, J = 9.4 Hz, 1H), 4.54 (d, J = 13.3 Hz, 1H), 4.11 (d, J = 9.5 Hz, 1H), 3.99 (q, J = 7.0 Hz, 2H), 3.61 (d, J = 13.3 Hz, 1H), 1.39 (t, J = 7.0 Hz, 3H). 13C NMR (150 MHz, CDCl3/CS2 (3:1 v/v)) δ 159.00, 156.08, 153.74, 153.26, 147.09, 147.08, 146.59, 146.22, 146.16, 146.11, 146.07, 146.00, 145.97, 145.93, 145.90, 145.73, 145.72, 145.57, 145.37, 145.33, 145.28, 145.22, 145.21, 145.09, 145.05, 145.03, 144.93, 144.51, 144.47, 144.19, 144.17, 142.96, 142.79, 142.48, 142.41, 142.37, 142.37, 142.14, 142.05, 141.96, 141.94, 141.91, 141.89, 141.83, 141.81, 141.76, 141.66, 141.45, 141.38, 140.00, 139.97, 139.78, 139.40, 136.68, 136.40, 135.67, 135.56, 130.29, 128.69, 128.60, 128.21, 127.46, 80.85(sp3-C of C60), 76.58(sp3-C of C60), 68.29, 66.35, 63.20, 56.57, 14.94. UV−vis (toluene) λ/(nm): 286, 336, 433. HRMS (MALDI-TOF) m/z calcd for C77H19NO [M + H]+ 973.1461, found 973.1455.

1H NMR spectra and 13C NMR spectra of compounds 2a-b.

Figure S1. 1H NMR (600 MHz, CS2/CDCl3) of compound 2a

Figure S2. 13C NMR (150 MHz, CS2/CDCl3) of compound 2a

Figure S2-1. Expanded 13C NMR (150 MHz, CS2/CDCl3) of compound 2a

Figure S2-2. Expanded 13C NMR (150 MHz, CS2/CDCl3) of compound 2a

Figure S2-3. Expanded 13C NMR (150 MHz, CS2/CDCl3) of compound 2a

Figure S3. 1H NMR (600 MHz, CS2/CDCl3) of compound 2b

Figure S4. 13C NMR (150 MHz, CS2/CDCl3) of compound 2b

Figure S4-1. Expanded 13C NMR (150 MHz, CS2/CDCl3) of compound 2b

Figure S4-2. Expanded 13C NMR (150 MHz, CS2/CDCl3) of compound 2b

Figure S4-3. Expanded 13C NMR (150 MHz, CS2/CDCl3) of compound 2b

HRMS of compounds 2a-b

The structures of products 2a-b were also fully characterized by MALDI-TOF mass. 2a: HRMS (MALDI-TOF) m/z calcd for C76H17NO [M + H]+ 959.1305, found 959.1309. 2b: HRMS (MALDI-TOF) m/z calcd for C77H19NO [M + H]+ 973.1461, found 973.1455.

Figure S5. High Performance Liquid Chromatography of 2a.

Figure S6. High Performance Liquid Chromatography of 2b.

HPLC of compounds 2a-b

Compounds 2a and 2b were purified by LC-9104 (Japan Analytical Industry Co. Ltd.) on a Buckyprep Waters 10×250 mm column. The mobile phase was toluene with a flow rate of 2 mL/min. The detection wavelength was at 330 nm. The retention time for 2a is about 13 min and 2b is about 12.5 min.

Figure S7. High Performance Liquid Chromatography of 2a.

Figure S8. High Performance Liquid Chromatography of 2b.

Water contact angle measurement of films

The contact angle test was performed by using a K100 tensiometer (Krüss Scientific Instruments). After a water drop fell to the surface of the film for 5 s, the static contact angle of films were tested.

Figure S9. Contact angle of PS film with water

Figure S10. Contact angle of 0.5%C60-PS film with water

Figure S11. Contact angle of 0.5%2a-PS film with water

Figure S12. Contact angle of 0.5%2b-PS film with water