Supporting Information for:

Star-shaped Oligomers with Truxenone Center and Triphenylene Branches: Mesomorphism, Optical and Electronic Properties

Wen Zhang a, Wen-Hao Yu a, Chun Feng a, Shi-Kai Xiang a, Bi-Qin Wang a , Ke-Qing Zhao a, Hai-Liang Ni a,* and Ping Hu a,*

a College of Chemistry and Material Sciences, Sichuan Normal University, Chengdu, 610066, P.R. China.

*E-mail: nihl@sicnu.edu.cn; hp_x@163.com

Contents:

TGA curves of three oligomers............................................................................. S2

DSC curves of three oligomers..............................................................................S3

POM images of three oligomers.............................................................................S4

X-ray Diffractograms................................................................................................S5

Cyclic Voltammetry Results. ..................................................................................S8

UV-Vis and Fluorescence Data .............................................................................S8

1H and 13C NMR Spectra..........................................................................................S11

HRMS of three oligomers…………………………….………………………………………………………S21

- TGA

Fig. S1. TGA curves of three oligomers. The measurements were performed under a nitrogen atmosphere, with heating and cooling rates of 10 oC min-1.

- Differential scanning calorimetry (DSC) curves of three oligomers

Fig. S2. DSC curves of three oligomers. The measurements were performed under a nitrogen atmosphere, with heating and cooling rates of 10 oC min-1.

- Polarizing optical microscopy images

(a)

(b)

(c)

Fig. S3. Polarized optical microscopy (POM) images of the drop-casted thin film of  three oligomers between two glass slides observed under two crossed polarizers upon slow cooling (1-2 oC min-1) from the isotropic phase: (a) TrO[O(CH2)6OTP]3 at 168 oC; (b) TrO[O(CH2)8OTP]3 at 158 oC; (c) TrO[O(CH2)10OTP]3 at 147 oC.

- X-ray diffraction (XRD)

Fig. S4. XRD data for three oligomers.

5. Cyclic Voltammogram

Fig. S5. Cyclic Voltammogram of three oligomers (2 mM) in dry DCM with 0.1 M Bu4NPF6 as the electrolyte with a scan rate of 100 mV s-1.

6. UV-Vis and Fluorescence Data

Fig. S6. UV-Vis absorbance spectra of 10-5 M solutions of three oligomers.

Fig. S7. Emission spectra of 10-5 M solutions of three oligomers (λexc = 350 nm).

Fig. S8. Fluorescence emission of TrO[O(CH2)6OTP]3 in different concentrations of DCM solution (λexc = 350 nm).

Fig. S9. Emission spectra of three oligomers in thin film (λexc = 350 nm).

7.  1HNMR and 13C NMR of 1, 2a-c and three oligomers

1H NMR spectrum of compound 1

1H NMR spectrum of compound 2a

1H NMR spectrum of compound 2b

1H NMR spectrum of compound 2c

1H NMR spectrum of compound TrO[O(CH2)6OTP]3

13C NMR spectrum of compound of TrO[O(CH2)6OTP]3

1H NMR spectrum of compound TrO[O(CH2)8OTP]3

13C NMR spectrum of compound of TrO[O(CH2)8OTP]3

1H NMR spectrum of compound TrO[O(CH2)10OTP]3

13C NMR spectrum of compound of TrO[O(CH2)10OTP]3

8. HRMS of three oligomers

TrO[O(CH2)6OTP]3

TrO[O(CH2)8OTP]3

TrO[O(CH2)10OTP]3