EVALUATION AND CHARACTERIZATION OF ALGAL BIOMASS APPLIED TO THE DEVELOPMENT OF FINGERMARKS ON GLASS SURFACES

Table 1S. Chemical components (% of area) of the biomass of the studied marine organisms.

| Compounds | Chlorella sp. | D. anceps | L. dendroidea | L. searlesiana | Spirulina sp. |
| --- | --- | --- | --- | --- | --- |
| Lactic acid | 1.08 ± 0.04ab | 0.36 ± 0.03ab | ndb | 0.28 ± 0.05ab | 1.15 ± 0.03a |
| Acetic acid | 0.37 ± 0.08a | 0.49 ± 0.08a | 2.80 ± 0.22b | 0.39 ± 0.04a | 0.24 ± 0.05a |
| Hydroxybutyric acid | 0.62 ± 0.02a | nda | nda | nda | 0.54 ± 0.05a |
| Hydroxyvaleric acid | 0.51 ± 0.03a | nda | nda | nda | nda |
| Succinic acid | 1.64 ± 0.25a | 0.19 ± 0.00b | ndb | ndb | ndb |
| Benzenepropanoic acid | 1.85 ± 0.04a | ndb | ndb | ndb | 0.24 ± 0.03b |
| Hydroxyhydrocinnamic acid | 0.41 ± 0.04a | nda | nda | nda | nda |
| Tetradecanoic acid | 0.58 ± 0.10a | nda | 2.34 ± 0.09b | nda | nda |
| Docosahexaenoic acid | 0.50 ± 0.04a | nda | nda | nda | 0.44 ± 0.05a |
| Palmitoleic acid | 8.12 ± 0.19a | ndc | ndc | ndc | 2.32 ± 0.29b |
| Hexadecanoic acid | 9.76 ± 0.34a | 0.46 ± 0.08c | 14.56 ± 0.05b | 0.46 ± 0.10c | 9.40 ± 0.60a |
| Linoleic acid | 25.31 ± 0.34a | ndb | ndb | 0.24 ± 0.08a | ndb |
| Linolenic acid | nda | nda | nda | nda | 5.75 ± 0.56b |
| Oleic acid | nda | nda | 1.42 ± 0.20a | nda | nda |
| Octadecanoic acid | 0.47 ± 0.03a | nda | 0.70 ± 0.18a | 0.17 ± 0.04a | nda |
| Glycerol monopalmitolate | 0.19± 0.05a | nda | nda | 0.18 ± 0.02a | 0.59 ± 0.46a |
| Glycerol monostearate | nda | nda | nda | nda | 0.22 ± 0.27a |
| Carboxylic acids | 50.94 ± 0.83a | 1.52 ± 0.20c | 21.82 ± 0.34b | 1.73 ± 0.11c | 20.93 ± 0.77b |
| Alanine | 1.57 ± 0.14a | 1.57 ± 0.23a | ndb | ndb | 0.36 ± 0.15b |
| L-norvaline | 0.68 ± 0.05a | nda | nda | nda | nda |
| Aminocaproic acid | 0.40 ± 0.04a | 0.06 ± 0.01a | nda | nda | nda |
| Amines | 2.66 ± 0.16a | 1.63 ± 0.22a | ndb | ndb | 0.36 ± 0.15b |
| Heptadecane | 0.40 ± 0.03a | nda | nda | nda | 1.15 ± 0.11b |
| Hydrocarbons | 0.40 ± 0.03a | nda | nda | nda | 1.15 ± 0.11b |
| Glycerol | 10.19 ± 0.14a | ndd | 1.52 ± 0.41c | 1.69 ± 0.02c | 5.82 ± 0.07b |
| 3,7,11,15-Tetramethyl-2-hexadecen-1-ol | 1.86 ± 0.14a | ndb | ndb | ndb | 0.23 ± 0.02b |
| Phytol | 2.89 ± 0.16a | ndb | ndb | ndb | 0.94 ± 0.10b |
| Glycerolgalactopyranoside | 1.76 ± 0.37a | ndb | ndb | ndb | ndb |
| Deoxyglucose | 2.23 ± 0.26a | nda | nda | nda | nda |
| Glycerophosphoric acid | 2.56 ± 0.50a | ndb | ndb | ndb | 0.24 ± 0.08b |
| 3,7,11,15-Tetramethyl-2-hexadecen-1-ol | 4.36 ± 0.30a | 0.54 ± 0.14bc | ndc | 0.27 ± 0.03c | 1.60 ± 0.19b |
| 3,7,11-Trimethyl-1-dodecanol | 0.43 ± 0.09a | nda | nda | nda | 0.19 ± 0.05a |
| D-turanose | 2.08± 0.37a | ndb | ndb | ndb | ndb |
| Erythro-pentofuranose | nda | nda | nda | nda | 0.27 ± 0.12a |
| Deoxy-galactose | nda | nda | nda | nda | 21.64 ± 2.59b |
| Glycerol-galactopyranose | nda | nda | nda | nda | 14.13 ± 2.81b |
| Unknown carbohydrate | nda | 79.19 ± 3.15b | nda | 81.77 ± 2.48b | nda |
| Elatol | nda | nda | 53.35 ± 1.47b | nda | nda |
| Alcohols | 28.39 ± 1.47a | 79.73 ± 3.01d | 55.06 ± 1.06c | 83.74 ± 2.42e | 45.08 ± 0.26b |
| Cholesterol | 0.92 ± 0.00a | nda | 5.22 ± 0.22b | nda | 0.38 ±0.03a |
| Ergosterol | 1.45 ± 0.11a | ndb | ndb | ndb | ndb |
| Fucosterol | nda | 2.57 ± 0.56b | nda | 2.77 ± 0.07b | nda |
| Steroids | 2.38 ± 0.11a | 2.57 ± 0.56a | 5.22 ± 0.22c | 2.77 ± 0.07a | 0.38 ± 0.03b |
| Unidentified | 14.71 ± 1.12 | 14.55 ± 2.03 | 17.88 ± 1.62 | 11.75 ± 2.46 | 32.08 ± 0.55 |
| Results expressed as mean ± standard deviation of triplicates (n=3) Different superscript letters indicate significant differences (p<0.05) |  |  |  |  |  |

Table 2S. Results of the IR Spectroscopy analysis of the samples.

| Bonding (cm-1) | Chlorella sp. | D. anceps | L. dendroidea | L. searlesiana | Spirulina sp. |
| --- | --- | --- | --- | --- | --- |
| -O-H | 3280 | 3240 | 3303 | 3253 | 3280 |
| =C-H | - | 3022 | 3022 | 3022 | - |
| -C-H | 2918 | 2968 | 2973 | 2973 | 2954 2923 |
| -C=O (ester) | 1737 | 1737 | 1737 | 1737 | - |
| -O-H (bending) | - | - | 1418 | - | - |
| -C=O (amide) | 1643 | - | - | - | 1650 |
| -N-H (amide) | 1536 | - | - | - | 1540 |
| -C-H (bending) | 1454 | 1366 | 1368 | 1366 | 1450 |
| -C-N | 1230 | 1228 | 1228 | 1228 | 1233 |
| -C-O | 1217 1027 | 1215 1208 1079 1020 | 1217 1206 1138 1124 1095 1025 | 1217 106 | 1020 |
| -C-Cl | - |  | 875 |  | - |
| -C-Br | - |  | 656 |  | - |

Table 3S. Particle size distribution of the studied marine biomasses.

| Samples | 10% (μm) | 50% (μm) | 90% (μm) |
| --- | --- | --- | --- |
| Chlorella sp. | 23.56 | 84.73 | 192.80 |
| D. anceps | 14.58 | 86.49 | 243.98 |
| L. dendroidea | 15.67 | 84.86 | 195.18 |
| L. searleasiana | 21.69 | 140.00 | 350.92 |
| Spirulina sp. | 8.66 | 42.18 | 148.00 |
| Commercial developer | 2.73 | 28.43 | 42.87 |

Table 4S. Superficial elementary composition of the studied marine biomasses.

| Elements (%) | Samples |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Chlorella sp. | D. anceps | L. dendroidea | L. searlesiana |  | Spirulina sp. |  |
| Si | - | - | 0.6 |  | - |  | - |
| P | 14.54 | 0.51 | - |  | 0.29 |  | 11.57 |
| S | 7.37 | 2.08 | 4.45 |  | 1.5 |  | 10.91 |
| Cl | - | 46.54 | 45.84 |  | 37.94 |  | - |
| K | 23.3 | 41.3 | 9.63 |  | 51.83 |  | 45.59 |
| Ca | 40.62 | 8.3 | 36.19 |  | 5.98 |  | 22.44 |
| Ti | 0.56 | - | 0.13 |  | - |  | - |
| Mn | 0.3 | - | - |  | - |  | 0.2 |
| Fe | 12.85 | 0.24 | 0.81 |  | 0.06 |  | 7.08 |
| Cu | 0.16 | 0.05 | 0.04 |  | 0.03 |  | 0.19 |
| Zn | 0.12 | 0.07 | - |  | - |  | - |
| As | - | 0.03 | - |  | 0.04 |  | - |
| Br | - | 0.33 | 2.05 |  | 1.42 |  | - |
| Rb | - | - | - |  | 0.06 |  | - |
| Sr | 0.19 | 0.47 | 0.18 |  | 0.3 |  | 0.13 |
| Zr | - | - | 0.04 |  | - |  | - |
| Ag | - | 0.04 | - |  | 0.06 |  | - |
| I | - | - | 0.05 |  | 0.48 |  | - |
| Ba | - | - | - |  | - |  | 1.89 |
| Pa | - | 0.03 | - |  | - |  | - |

Figure 1S. FT-IR spectrum of all the algae biomasses.

Figure 2S. GC-MS chromatogram of the extract from the biomass of Chlorella sp.

Figure 3S. GC-MS chromatogram of the extract from the biomass of Spirulina sp.

Figure 4S. GC-MS chromatogram of the extract from the biomass of L. dendroidea.

Figure 5S. GC-MS chromatogram of the extract from the biomass of D. anceps.

Figure 6S. GC-MS chromatogram of the extract from the biomass of L. searlesiana.

Figure 7S. Depletion study using Spirulina sp. biomass under 24 hours for natural latent fingerprint

Figure 8S. Depletion study using Spirulina sp. biomass under 72 hours for natural latent fingerprint

Figure 9S. Depletion study using Spirulina sp. biomass under 24 hours for sebaceous latent fingerprint.

Figure 10S. Depletion study using Spirulina sp. biomass under 72 hours for sebaceous latent fingerprint