Supplementary information

Journal of Wood Chemistry and Technology

A bio-based adhesive composed of polyelectrolyte complexes of lignosulfonate and cationic polyelectrolytes

Kazunori Ushimaru, Tomotake Morita, Tokuma Fukuoka*

Research Institute for Sustainable Chemistry, National Institute of Advanced Industrial Science and Technology (AIST), Tsukuba Central 5-2, 1-1-1 Higashi, Tsukuba, Ibaraki 305-8565, Japan

Corresponding author, Tokuma Fukuoka

Tel.: +81 29 861 4427

E-mail address: t-fukuoka@aist.go.jp

Supporting Table S1. The stoichiometry of the anionic and cationic functional groups in the L-SO3Na/cationic-polyelectrolyte complexes.

| Complex | L-SO3Na (wt%) | Cationic polyelectrolyte (wt%) | Ratio of anionic/cationic functional groups in the complex |
| --- | --- | --- | --- |
| L-SO3Na/PAA | 50 | 50 | 1:5.6 |
|  | 40 | 60 | 1:8.5 |
| L-SO3Na/-PL | 50 | 50 | 1:2.6 |
|  | 40 | 60 | 1:3.9 |
| L-SO3Na /PDADMACl | 50 | 50 | 1:2.0 |
|  | 40 | 60 | 1:3.0 |
| The molar concentration of functional groups in L-SO3Na and cationic polyelectrolytes were calculated from the result of elemental analysis of L-SO3Na in reference 8 and molecular structure of the cationic polyelectrolytes. |

Supporting Figure S1(a)

Supporting Figure S1(b)

Supporting Figure S1(c)

Supporting Figure S1. Photographs of specimens after shear adhesion testing using PDADMACl_60 adhesive on (a) aluminum and (b) wood. The photograph in (c) shows a commercial polyvinyl acetate adhesive on wood.