Table1S. ANOVA table of the indicators in the study.

| Factor |  | Mean square | F value |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | No. | Block (B) | Hybrids (H) | B×H | Density (D) | D×H | Block (B) | Hybrids (H) | B×H | Density (D) | D×H |
| DF |  | 2 | 5 | 10 | 2 | 10 | 2 | 5 | 10 | 2 | 10 |
| Stem dry weight per length: g cm-1 | 1st | 0.05 | 0.15 | 0.02 | 1.75 | 0.01 | 2.36ns | 7.78** | 2.46ns | 223.22** | 0.81ns |
|  | 2nd | 0.00 | 0.11 | 0.00 | 0.81 | 0.00 | 0.37ns | 44.88** | 2.27ns | 747.84** | 3.29** |
|  | 3rd | 0.01 | 0.06 | 0.00 | 1.00 | 0.01 | 0.81ns | 93.68** | 0.54ns | 799.07** | 5.31** |
|  | 4th | 0.00 | 0.05 | 0.00 | 0.37 | 0.00 | 1.19ns | 25.31** | 1.71ns | 301.91** | 1.27ns |
|  | 5th | 0.00 | 0.05 | 0.00 | 0.25 | 0.00 | 1.14ns | 60.57** | 0.95ns | 286.96** | 3.23** |
| Stem rind puncture strength: N | 1st | 33.37 | 436.63 | 10.81 | 774.98 | 13.32 | 3.09ns | 40.39** | 1.67ns | 119.81** | 2.06ns |
|  | 2nd | 0.05 | 594.71 | 10.21 | 2013.50 | 10.69 | 0.01ns | 58.27** | 0.95ns | 186.79** | 0.99ns |
|  | 3rd | 1.60 | 378.13 | 6.86 | 2033.31 | 8.78 | 0.23ns | 55.14** | 0.46ns | 137.66** | 0.59ns |
|  | 4th | 12.65 | 504.38 | 14.19 | 2483.48 | 49.19 | 0.89ns | 35.55** | 1.32ns | 231.33** | 4.58** |
|  | 5th | 7.51 | 521.89 | 4.87 | 1745.05 | 85.97 | 1.54ns | 107.21** | 0.25ns | 90.55** | 4.46** |
| Stem crushing strength: kg | 1st | 31.57 | 176.18 | 11.79 | 3201.86 | 21.19 | 2.68ns | 14.95** | 0.74ns | 202.01** | 1.34ns |
|  | 2nd | 8.25 | 456.54 | 7.75 | 2120.20 | 8.35 | 1.06ns | 58.92** | 0.53ns | 145.42** | 0.57ns |
|  | 3rd | 26.20 | 256.86 | 9.33 | 5789.63 | 17.59 | 2.81ns | 27.53** | 1.19ns | 736.92** | 2.24ns |
|  | 4rd | 42.45 | 223.88 | 9.96 | 1966.02 | 21.79 | 4.26ns | 22.49** | 1.30ns | 256.82** | 2.85* |
|  | 5th | 3.78 | 238.74 | 6.68 | 1547.62 | 14.70 | 0.57ns | 35.74** | 1.29ns | 299.38** | 2.84* |
| Stem bending strength: N | 3rd | 9.88 | 1167.44 | 13.56 | 4998.12 | 42.50 | 0.73ns | 86.08** | 1.95ns | 720.13** | 6.12** |
|  | 4rd | 49.59 | 549.06 | 14.56 | 2601.01 | 15.45 | 3.41ns | 37.71** | 1.44ns | 256.66** | 1.52ns |
|  | 5th | 23.10 | 196.33 | 12.58 | 1086.61 | 20.30 | 1.84ns | 15.61** | 2.37ns | 204.57** | 3.82** |

Block, Hybrids and Density are abbreviated B, H and D, respectively, in the interaction terms. ns: not significant (P>0.05); *, **: significant at P < 0.05 and P < 0.01, respectively.

Supplementary information

Figure 1S. Accumulated rainfall (mm) and average temperature (T, °C) every 10 days during maize growth season in 2016 and 2017.

Figure 2S. Genotypic difference in stem dry weight per length of the 1st, 2nd, 3rd, 4th, 5th node in response to plant density across two experimental years. Bars denote the SE of the mean (n=3). Different lowercase letters represent significant differences among hybrids under the same planting density (P < 0.05). Different capital letters represent significant differences among planting densities across all the hybrids (P < 0.05).

Figure 3S. Genotypic difference in rind penetration strength of the 1st, 2nd, 3rd, 4th, 5th node in response to plant density across two experimental years. Bars denote the SE of the mean (n=3). Different lowercase letters represent significant differences among hybrids under the same planting density (P < 0.05). Different capital letters represent significant differences among planting densities across all the hybrids (P < 0.05).

Figure 4S. Genotypic difference in stem crushing strength of the 1st, 2nd, 3rd, 4th, 5th node in response to plant density across two experimental years. Bars denote the SE of the mean (n=3). Different lowercase letters represent significant differences among hybrids under the same planting density (P < 0.05). Different capital letters represent significant differences among planting densities across all the hybrids (P < 0.05).

Figure 5S. Genotypic difference in stem bending strength of the 3rd, 4th, 5th node in response to plant density across two experimental years. Bars denote the SE of the mean (n=3). Different lowercase letters represent significant differences among hybrids under the same planting density (P < 0.05). Different capital letters represent significant differences among planting densities across all the hybrids (P < 0.05).

Figure 6S. Genotypic differences in plant height, ear height to plant height ratio at three plant densities for two experimental years. Bars denote the SE of the mean (n=3). Different lowercase letters represent significant differences among hybrids under the same planting density (P < 0.05). Different capital letters represent significant differences among planting densities across all the hybrids (P < 0.05).

Figure 1S

Figure 2S

Figure 3S

Figure 4S

Figure 5S

Figure 6S