Supporting Information

# Removal of various pollutants from wastewaters using an efficient and degradable hypercrosslinked polymer

Zujin Yang1,3, Guifang Wu1, Qiuru Li2, Hongxia Ai2, Xingdong Yao4, Hongbing Ji2,3,5*

1 School of Chemical Engineering and Technology, Sun Yat-sen University, Zhuhai 519082, China

2 Fine Chemical Industry Research Institute, The Key Laboratory of Low-carbon Chemistry & Energy Conservation of Guangdong Province, School of Chemistry, Sun Yat-sen University, Guangzhou 510275, China

3 Huizhou Research Institute of Sun Yat-sen University, Huizhou 516216, China

4The Key laboratory of Forest Chemistry & Engineering of Guangxi, Guangxi University for Nationalities, Nanning, China

5 School of Chemical Engineering, Guangdong University of Petrochemical Technology, Maoming 525000, China

Adsorption Model Fitting

After adsorption, the concentration of aniline in the solution at a regular time interval was determined and the amount of the compound adsorbed by mass unit of adsorbent at t (qt, mg/g) was calculated by Eq (1) described in Section 2.3. In this work, nonlinear regression of pseudo-first order, pseudo-second order, and pseudo-nth-order equations were analyzed with the aid of commercial available software Sigma Plot 11(1).

(1) The pseudo-first order equation was widely used for adsorption process, and its equation is expressed as (2):

|  | (1) |
| --- | --- |

where qt and qe are adsorbed amount of aniline adsorbed at time t and at equilibrium (mg/g), respectively, and k1 is the rate constant of pseudo-first-order adsorption process (L/min).

The corresponding form in the equation of Sigma Plot 11“Exponential Rise to Maximum equation, Single, 2 Parameter” is given by,

|  | (2) |
| --- | --- |

The corresponding parameters are y = qt, a = qe, b = k1, and x = t.

The pseudo-second order equation based on equilibrium capacity is represented as (2):

|  | (3) |
| --- | --- |

where k2 is the equilibrium rate constant of pseudo-second-order adsorption(g/mg/min).

Eq (3) was rewritten to the corresponding form as Eq (4),

|  | (4) |
| --- | --- |

The corresponding parameters are y =, a =, b = 1/, and x = t.

Nonlinear forms of the pseudo-nth-order equation is expressed as (3),

(5)

The corresponding Sigma Plot’s form in equation category “Power equation, Modified Pareto Function” is,

(6)

The corresponding parameters are y =, a =, b=1/(n-1), and x = t.

The previous refs indicated that the value of n is between 1 and 2, implying that the curves are in the range of pseudo-first order and pseudo-second order equations (1, 4). If n is larger than 2, it showed that the curvatures of these curves are larger than those of pseudo-first order and pseudo-second order curves (5, 6).

The relative standard deviation (RSD) is defined by,

|  | (7) |
| --- | --- |

where N is the number of data points.

Nonlinear regression of experimental results to the Freundlich (2) and Langmuir (2) isotherms was determined in order to describe the equilibrium data of aniline adsorption on the 2-HTA-HCP.

The Langmuir equation is given as

|  | (8) |
| --- | --- |

where ce (mg/L) and qe (mg/g) are the concentration of adsorbate and adsorbed amount of the compound adsorbed at time t, respectively. KL is Langmuir adsorption constant and qm (mg/g) is the theoretical maximum adsorption amount to form monolayer on the polymer, respectively.

The Freundlich isotherm is used to describe multilayer adsorption with interaction between the adsorbed molecules, and is determined as:

|  | (9) |
| --- | --- |

where Kf is Freundlich constant that is an indicator of adsorption concentration and 1/n is the Freundlich coefficient related to the magnitude of the adsorption driving force.

Figures and Tables

Figure S1. TGA of 2-HTA-HCP

Figure S2. Effect of regeneration cycles on the adsorption capacity of p-ABA, p-MA, aniline, and p-CA via 2-HTA-HCP. Adsorption conditions: 2-HTA-HCP (0.1 g), initial concentration (100 mg/L), Vo (100 mL), 25 °C, 200 r/min, pH = 7, 720 min.

(a) 2-HTA/aniline BE2 = -24.57 kJ/mol   (b) 2-HTA/aniline BE2 = -27.24 kJ/mol

Figure S3. Optimized structure of 2-HTA/aniline by the DMol3.

Table S1. Comparison of the maximum uptake of Ni2+, Cu2+, Cd2+, and Pb2+ on various adsorbents.

| Adsorbent | Solution conditions | qmax (mg/g) | Refs. |
| --- | --- | --- | --- |
|  |  | Ni2+ | Cu2+ | Cd2+ | Pb2+ |  |
| Carbon nanotube/diatomite | pH = 6, T = 30 °C | - | - | - | 60 | (7) |
| Cellulose/chitosan composite | pH = 5, T = 25 °C | - | 33.03 | 31.47 | 33.16 | (8) |
| MNPs-COOH | pH = 5, T = 25 °C | 25.89 | 41.91 | 58.22 | 177.16 | (9) |
| P(AAm/CA)no imprinting hydrogel | pH = 6, T = 25 °C | 12.20 | 10.92 |  |  | (10) |
| P(AMPSG/AAc/NVP/HEMA) hydrogel | pH = 5, T = 25 °C |  |  | 27.76 | 22.79 | (11) |
| Chemical treated cherry kernels | pH = 6, T = 25 °C | 12.33 |  | 19.67 | 17.86 | (12) |

Table S2. Number, type, bond length (r), bond angle (A) and BE2 of intermolecular hydrogen bond between 2-HTA and aniline calculated by DMol3

| Inclusion complexes | Number | Type | r (Å) | A (o) | BE2(kJ/mol) |
| --- | --- | --- | --- | --- | --- |
| 2-HTA/aniline | 1 | N-H…O | 2.042 | 113.330 | -24.57 |
| 2-HTA/aniline | 1 | N-H…O | 1.613 | 123.379 | -27.24 |

References

(1) Tseng, R. L.; Wu, P. H.; Wu, F. C.; Juang, R. S. A convenient method to determine kinetic parameters of adsorption processes by nonlinear regression of pseudo-nth-order equation. Chem. Eng. J, 2014, 237, 153-161.

(2) Chingombe, P.; Saha, B.; Wakeman, R. J., Sorption of atrazine on conventional and surface modified activated carbons. J. Colloid. Interf. Sci, 2006, 302: 408-416.

(3) Özer, A. Removal of Pb(II) ions from aqueous solutions by sulphuric acid-treated wheat bran. J. Hazard. Mater, 2007, 141, 753-761.

(4) Leyva-Ramos, R.; Rivera-Utrilla, J.; Medellin-Castillo, N. A.; Sanchez-Polo, M. Kinetic modeling of fluoride adsorption from aqueous solution onto bone char. Chem. Eng. J, 2010, 158, 458-467.

(5) Morais, W. A.; Fernandes, A. L. P.; Dantas, T. N. C.; Pereira, M. R.; Fonseca, J. L. C. Sorption studies of a model anionic dye on crosslinked chitosan. Colloids. Surfaces. A: Physicochem. Eng. Aspects, 2007, 310, 20-31.

(6) Morais, W. A.; de Almeida, A. L. P.; Pereira, M. R.; Fonseca, J. L. C. Equilibrium and kinetic analysis of methyl orange sorption on chitosan spheres. Carbohy. Res, 2008, 343, 2489-2493.

(7) Alijani, H.; Beyki, M. H.; Shariatinia, Z.; Bayat, M.; Shemirani, F. A new approach for one step synthesis of magnetic carbon nanotubes/diatomite earth composite by chemical vapor deposition method: Application for removal of lead ions. Chem. Eng. J, 2014, 253: 456-463.

(8) Xiao, M.; Hu, J. Cellulose/chitosan composites prepared in ethylene diamine/potassium thiocyanate for adsorption of heavy metal ions. Cellulose, 2017, 24: 2545-2557.

(9) Xu, H.; Yuan, H.; Yu, J.; Lin, S. Study on the competitive adsorption and correlational mechanism for heavy metal ions using the carboxylated magnetic iron oxide nanoparticles (MNPs-COOH) as efficient adsorbents. Appl. Surf .Sci, 2019, 473: 960-966.

(10) Mahmoud, G. A.; Hegazy, E. A.; Badway, N. A.; Salam, K. M. M.; Elbakery, S. M., Radiation synthesis of imprinted hydrogels for selective metal ions adsorption. Desalin. Water. Treat, 2016, 57: 16540-16551.

(11) Yetimoğlu, E. K.; Fırlak, M.; Kahraman, M. V.; Deniz, S. Removal of Pb2+ and Cd2+ ions from aqueous solutions using guanidine modified hydrogels. Polym. Advan. Technol, 2011, 22: 612-619.

(12) Pap, S.; Radonić, J.; Trifunović, S.; Adamović, D.; Mihajlović, I.; Vojinović Miloradov, M.; Turk Sekulić, M., Evaluation of the adsorption potential of eco-friendly activated carbon prepared from cherry kernels for the removal of Pb2+, Cd2+ and Ni2+ from aqueous wastes. J. Environ. Manage, 2016, 184: 297-306.