Co-assembled ZnO-Fe2O3x-CuOx nano-oxide materials for antibacterial protection

S. J. Owonubi1, Collins N. Ateba2 and Neerish Revaprasadu1

1 Department of Chemistry, University of Zululand, KwaDlangezwa, KwaZulu-Natal, South Africa

2Department of Microbiology, Faculty of Natural and Agricultural Sciences, North-West University, Mafikeng Campus, Private Bag X2046, Mmabatho, 2735, South Africa

Email: oshesan@gmail.com

Supplemental Materials

Figure S 1: XRD spectra for MONPs

Figure S 2: TEM Micrographs of (a) ZnO (b) FeO (c) CuO (d) CuOFeO0.5

Figure S 3: SEM micrographs of (a) ZnO (b) FeO (c) CuO

Figure S 4: SEM micrographs, EDX pattern and mappings of (a) ZnOFeO0.5 CuO0.5 (b) ZnOFeO0.5 (c) CuOFeO0.5

Figure S 5: Antibacterial activity of synthesized MONPs treatments (1mg/mL) on S.pneumoniae

Table S 1: Antibacterial activity of synthesized MONPs treatments (1 mg/mL) on S.pneumoniae

| Zone of Inhibition Diameter (mm) ± SD |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | ZnO | Fe2O3 | CuO | CuOFeO0.5 | ZnOFeO0.5 | ZnOFeO0.1CuO0.1 | ZnOFeO0.5CuO0.5 |
| B.cereus | - | - | 16 ± 0.3 | 26 ± 0.2 | - | 20 ± 1.4 | 24 ± 0.8 |
| S.pneumoniae | - | 8 ± 0.67 | 31 ± 0.5 | 25 ± 0.8 | - | 20 ± 0.5 | 28 ± 1.1 |
| S.aureus | - | - | 27 ± 0.7 | 28 ± 0.6 | - | - | 29 ± 0.5 |