Supporting Information

Dual-responsive targeted hollow mesoporous silica nanoparticles for cancer photodynamic therapy and chemotherapy

Yuqi Chena,1, Xuelian Wangb,1, Zhuhang Lub, Cong Changb, Yueli Zhanga, Bo Lua, *

aSchool of Chemistry, Chemical Engineering and Life Sciences, Wuhan University of Technology, Wuhan 430070, PR China.

bCollege of Pharmacy, Hubei University of Chinese Medicine, Wuhan, PR China.

*Corresponding author.

E-mail: lvb@whut.edu.cn

Tel & Fax: 086-027-87749300

1These authors contributed equally to this work.

Figure S1. Hydrodynamic diameter distributions of HMSNs and HMSNs-CS-HDA.

Figure S2. XRD of HMSNs and DOX@HMSNs-CS-HAD.

Figure S3. BJH pore size distributions of HMSNs and HMSNs-CS-HAD.

Figure S4. L02 cells incubated with free DOX+ICG and ID@HCH.

Table S1 BET and BJH parameters of HMSNs and HMSNs-CS-HDA.

| Sample | BET surface area SBET (m² g-1) | BJH pore volume VP (cm³ g-1) | BJH pore diameter VBJH (nm) |
| --- | --- | --- | --- |
| HMSNs | 956 | 1.34 | 5.59 |
| HMSNs-CS-HDA | 70 | 0.18 | / |

Table S2 IC50 values of various HMSNs on HepG2 cells after 24 h.

|  | Free DOX (μg mL-1) | ICG+DOX + laser (μg mL-1) | DOX@HCH (μg mL-1) | ID@HCH+ laser (μg mL-1) |
| --- | --- | --- | --- | --- |
| HepG2 cells | 0.49 | 0.44 | 0.28 | 0.12 |